Hydroxyapatite Nano-Fertilizers Effects on Adsorption and Uptake of Cadmium and Lead, Nutrient Release and Growth Performance of Selected Crops

Ngorwe Evans Nyaenya (M Sc)

I84/28935/2013

A Thesis Submitted in Fulfillment of the Requirements for the Award of the Degree of Doctor of Philosophy (Chemistry) in the School of Pure and Applied Sciences of Kenyatta University,September, 2023.
Declaration

I hereby declare that this is my original work and has not been presented for degree or other awards in any other university

Ngorwe Evans Nyaenya

I84/28935/2013

Department of Chemistry

Sign _________________________Date _____________________________

SUPERVISORS

We confirm that the work reported in this thesis was carried by the student under our supervision.

Prof. Hudson Nyambaka,

Department of Chemistry,

Kenyatta University.

Sign __________________________                  Date_______________________

Dr. Mildred P. Nawiri,

Department of Chemistry,

Kenyatta University.

Sign __________________________                  Date_______________________

Prof. Jane Murungi,

Department of Chemistry,

Kenyatta University.

Sign __________________________                  Date_______________________

# DEDICATION

To my wife Ongera Tabitha, daughter Flavian Bonareri, sons Adrian Nyaenya, Fabian Ongera and Aidan Momanyi, together with my father Wilfred Nyaenya and mother Teresia Kerubo whom am indebted by their encouragement, moral support and insightful ideas, that made this study a reality.

# ACKNOWLEDGEMENTS

Lots of gratitude goes to my supervisors Dr. Mildred Nawiri, Prof. Jane Murungi and Prof. Hudson Nyambaka for their encouragement, close supervision and insightful ideas in course of my study. My gratitude also goes to the Kenyatta University’s Chemistry departmental lecturers, for their insightful ideas during my departmental presentations and defense. Special thanks go to the Kenyatta University technicians, Dr. Jane Mburu and Mr. John Kariuki who assisted me with AAS, UV, XRD, SEM, FTIR and their technical support during the lab work analysis. I am also grateful to IOSR Journal of Applied Chemistry (IOSR-JAC) and International Journal of Science & Technoledge (IJST) journals for publishing part of my work.

In addition, special thanks go to my dad Wilfred Nyaenya, mum Teresia Kerubo, brothers Gilly Maranga, Peter Otwori, Alex Nyamosi, Andrey Momanyi and sisters’ Judy Kwamboka, Hyline Kerubo, Jossy Moraa for their unquantified moral and financial support. Not forgetting my friends, Kevin Omollo, Samuel Ndungu and Edwin Nyangau, whom we collaborated working in the laboratories. Lastly am indebted to my Spouse, Mrs. Nyanchoka Tabitha and beloved kids; daughter Flavian Bonareri and sons Adrian Nyaenya, Fabian Ongera and Aidan Momanyi whom I am venerated for their love and patience, during the entire period I was undertaking my PhD studies.

# TABLE OF CONTENTS

SEPTEMBER, 2023DECLARATION	i

DEDICATION	iii

ACKNOWLEDGEMENTS	iv

TABLE OF CONTENTS	v

LIST OF TABLES	xi

LIST OF FIGURES	xiii

LIST OF ABBREVITIONS AND ACRONYMS	xv

ABSTRACT	xvi

CHAPTER ONE	1

INTRODUCTION	1

1.1 Background Information	1

1.2 Statement of the Problem and Justification	5

1.3 Null Hypotheses	7

1.4 Objectives	7

1.4.1 General Objective	7

1.4.2 Specific Objectives	7

1.5 Significance of the Study	8

1.6 Scope and Limitation	9

CHAPTER TWO	10

LITERATURE REVIEW	10

2.1 Commercial Fertilizers in Crop Production	10

2.2 Nano-fertilizers	11

2.3 Effects of Nano fertilizer on Cd and Pb Uptake	12

2.4 Hydroxyapatite Nano fertilizers and their Heavy Metal Immobilization in Plants	14

2.5 Effect of Nano fertilizers on Plant Growth Performance	17

2.6 Nano-fertilizer Thermodynamics	19

2.7 Effects of Experimental Conditions on Adsorption of Cd and Pb	21

2.7.1 Effect of Soil pH on Adsorption of Cd and Pb	21

2.7.2 Effect of Adsorbent Dosage on Adsorption of Cd and Pb	21

2.7.3 Effect of Contact Time on Adsorption of Cd and Pb	22

2.7.4 Effect of Initial Metal Ion Concentration on Adsorption of Cd and Pb	23

2.7.5 Adsorption Isotherms	23

2.7.6 Adsorption Kinetics	25

2.8 Analytical Methods	26

2.8.1 Atomic Absorption Spectroscopy	26

2.8.2 Nanoparticle Characterization Methods	27

2.8.2.1 Fourier Transform Infrared Spectroscopy	27

2.8.2.2 Scanning Electron Microscopy	29

2.8.2.3 X-Ray Diffraction	29

CHAPTER THREE	31

METHODOLOGY	31

3.1 Research Design	31

3.2 Reagents and Chemicals	31

3.3 Method Validation	32

3.3.1 Recovery Tests	32

3.3.2 Limit of Detection of AAS	32

3.4 Synthesis of Hydroxyapatite Nano-fertilizers	32

3.4.1 Synthesis of Synthetic nHA Nano-fertilizers	32

3.4.2 Synthesis of Bone nHA Nano-fertilizers	33

3.5 Nanoparticle Characterization	34

3.6 Determination of Cd and Pb Uptake in Kale, Spinach and Beans	35

3.6.1 Harvesting of Plant Samples	36

3.6.2 Preparation of Standards	36

3.6.3 Sample Digestion and Heavy Metal Determination	37

3.7 Determination of Growth Performance	38

3.7.1 Plant Height	38

3.7.2 Leaf Diameter	38

3.7.3 Number of Leaves	38

3.7.4 Number of Pods	39

3.7.5 Dry Biomass Weight	39

3.8 Determination of Adsorption Capacity of Nanofertilizers	39

3.8.1 Effect of pH on Removal of Metal	39

3.8.2 Effect of Initial Metal Concentration on Removal of Metal	40

3.8.3 Effect of Contact Time on Removal of Metal	40

3.8.4 Effect of Adsorbent Dosage on Removal of Metal	41

3.9 Adsorption and Kinetic Studies	41

3.10 Nutrients Release Levels by Nano-fertilizers	42

3.11 Data Analysis	42

CHAPTER FOUR	44

RESULTS AND DISCUSSIONS	44

4.1 Introduction	44

4.2 Method Validation	44

4.3 Nanoparticle Characterization	45

4.3.1 SEM Analysis	45

4.3.2 XRD Analysis	47

4.3.3 FTIR Analysis	50

4.4 Cadmium and Lead Uptake	53

4.4.1 Uptake Levels of Cd in Crops Grown Using Nano-fertilizers	53

4.4.2 Uptake Levels of Pb in Plant Leaves Grown Using Nano-fertilizers	60

4.5 Growth Performance of Crops Grown Using Nano-fertilizers	65

4.5.1 Plant Height Growth Performance	65

4.5.2 Dry Weight, Leaf Diameter and Plant Number of Leaves	70

4.6 Effects of Experimental Conditions on Adsorption of Metal	75

4.6.1 Effect of Initial pH on Removal of Metal ion by Nanofertilizers	75

4.6.2 Effect of Nano-adsorbent Dose on Removal of Metal by Nanofertilizers	76

4.6.3 Effect of Initial Metal Concentration on Adsorption by Nanofertilizers	77

4.6.4 Effect of Contact Time on Adsorption of Metal by Nanofertilizers	78

4.7 Adsorption Isotherms after Optimization	79

4.8 Adsorption Isotherms Fitting for Cadmium and Lead	80

4.8.1 Adsorption Isotherms Fitting for Cadmium	80

4.8.2 Adsorption Isotherms Fitting for Lead	81

4.9 Adsorption Kinetic Studies	83

4.9.1 Adsorption Kinetic Studies for Cadmium and Lead	83

4.10 Nutrient Release Concentration Studies	86

CHAPTER FIVE	93

CONCLUSIONS AND RECOMMENDATIONS	93

5.1 Conclusions	93

5.2.1 Recommendations from the Study	94

5.2.2 Recommendation for Further Research	94

REFERENCES	95

APPENDICES	103

Appendix I: Percentage Pb and Cd reduction uptake in kales, spinach and beans at maturity (After 90 days)	103

Appendix II: Percentage effect on height growth performance of kales, spinach and beans at maturity (After 90 days)	104

Appendix III: % Phosphate release rate in bone and synthetic nHA nano-fertilizer	105

Appendix IV: % Phosphate release rate in bone and synthetic nHA nano-fertilizer	106

Appendix V: Published paper With IOSR-JAC.	107

Appendix VI: Published paper With IJSR	108

Appendix VII: Approval of Research Proposal	109

Appendix VIII: Research Authorization	110

# LIST OF TABLES

Table 4.1: Method Validation parameters	44

Table 4.2: Nano-fertilizer particle sizes determined from XRD analysis	50

Table 4.3: Levels of cadmium in kale leaves grown using nano-fertilizers at 30, 60 and 90 day	54

Table 4.4: Levels of cadmium in spinach leaves grown using nano-fertilizers at 30, 60 and 90 day	55

Table 4.5: Levels of cadmium in bean leaves grown using nano-fertilizers at 30, 60 and 90 day	56

Table 4.6: Comparison of cadmium uptake in bean, kale and spinach leaves grown using nano-fertilizers at 90th day	57

Table 4.7: Levels of lead in kale leave grown using nano-fertilizers at 30, 60 and 90 day	60

Table 4.8: Levels of lead in spinach leaves grown using nano-fertilizers at 30, 60 and 90 day	61

Table 4.9: Levels of lead in bean leaves grown using nano-fertilizers at 30, 60 and 90 day	62

Table 4.10: Comparison of lead uptake in bean, kale and spinach leaves grown using nano-fertilizers at 90th day	63

Table 4.11: The 30, 60, 90 day Heights (cm) for kales grown using nano-fertilizers	66

Table 4.12: The 30, 60, 90 day Heights (cm) for spinach grown using nano-fertilizers	67

Table 4.13: The 30, 60, 90 day Heights (cm) for bean grown using nano-fertilizers	68

Table 4.14: The 90 day dry weight, leaf diameter and number of leaves in kales grown using nano-fertilizers	71

Table 4.15: The 90 day dry weight, leaf diameter, number of pods and number of leaves in beans grown using nano-fertilizers	72

Table 4.16: The 90 day dry weight, leaf diameter and number of leaves in spinach grown using nano-fertilizers	73

Table 4.17: Langmuir and Freundlich Cd2+adsorption isotherm parameter models	80

Table 4.18: Results of Langmuir and Freundlich adsorption isotherm parameter model for Pb2+	82

Table 4.19: Computed results of adsorption kinetic using pseudo first order equation	84

Table 4.20: Second order pseudo kinetic parameters	85

Table 4.21: Nitrate nutrient release concentrations by nano-fertilizers and commercial fertilizers	87

Table 4.22: Phosphate nutrient release concentrations by nano-fertilizers and commercial fertilizers	88

Table 4.23: Potassium nutrient release concentrations by nano-fertilizers and conventional fertilizers	89

# LIST OF FIGURES

Figure 4.1: (a) SEM image of bone nHA and (b) SEM image of synthetic nHA	45

Figure 4.2: (a) SEM image of bone DAP Nano and (b) SEM image of synthetic DAP Nano	45

Figure 4.3: (a) SEM image of bone NPK Nano and (b) SEM image of synthetic NPK Nano	46

Figure 4.4: (a): XRD image of bone nHA and (b) XRD image of synthetic nHA	47

Figure 4.5: (a): XRD image of bone DAP Nano and (b) XRD image of synthetic DAP Nano	48

Figure 4.6: (a) XRD image of bone NPK nano and (b) XRD image of synthetic NPK Nano	48

Figure 4.7: (a) XRD image of bone NPK-DAP Nano and (b) XRD image of synthetic NPK-DAP Nano	49

Figure 4.8: FTIR images of various nanofertilizers in the order (a) bone nHA, (b)synthetic nHA, (c)bone DAP nano, (d) synthetic DAP nano, (e) bone NPK nano, (f) synthetic NPK nano,(g) bone NPK-DAP nano, (h) synthetic NPK-DAP nano respectively.	52

Figure 4.9: pH change and the adsorption of Cd2+ and Pb2+ on bone nHA	76

Figure 4.10: Adsorbent dosage on Pb2+ adsorption using bone nHA	77

Figure 4.11: Effect of Initial metal concentration on removal of Cd2+ and Pb2+ on bone nHA	78

Figure 4.12: Contact time on the adsorption of Cd2+ and Pb2+ on bone nHA	79

Figure 4.13: Graph on NO3- released by Bone nHA nanofertilizers within 40 days	91

Figure 4.14: Graph on NO3-- release by synthetic nHA nanofertilizers within 40 days	91

Figure 4.15: Graph on NO3- release by commercial fertilizers within 40 days	92

# LIST OF ABBREVITIONS AND ACRONYMS

| AAS | Atomic Absorption Spectrometry |
| --- | --- |
| ANOVA | Analysis of Variance |
| DAP | Di-ammonium Phosphate |
| EC | Electrical Conductivity |
| FAO | Food and Agriculture Organization |
| FTIR | Fourier Transform Infra Red |
| HA | Hydroxyapatite |
| MDL | Method Detection Limit |
| nHA | Nanohydroxyapatites |
| NPK | Nitrogen Phosphorus Potassium fertilizer |
| SEM | Scanning Electron Microscopy |
| SIDs | Sudden Infant Death Syndrome |
| SNK | Student-Newman-Kuels test |
| Syn | Synthetic |
| WHO | World Health Organization |
| XRD | X- Ray Diffractometry |

# ABSTRACT

More than 9.1 million people globally are affected by famine. Spinach, kales and beans are among vegetables promoted for consumption as an intervention strategy. Until the development of nanofertilizers such as synthetic hydroxyapatite (Syn nHA), boosting vegetable production has been by employing commercial and organic fertilizers. Other than being micro-sized, nanofertilizers have reduced uptake of harmful heavy metals like Pb, Cd, and improved growth performance (height, dry weight, leaf diameter and number of leaves) of crops due to their numerous adsorption sites. Further advantages include, being stable, non-toxic and having enhanced surface area to volume ratio. Use of over 130 billion tones of bone being dumped per year to prepare nanofertilizers is likely to reduce its environmental menace. This study envisaged using bones to synthesize nanofertilizers (bone nHA) and. investigated the effect of bone nHA and Syn nHA nano-fertilizers on Cd and Pb uptake and adsorption, growth performance, and nutrient release in beans, spinach and kale leaves grown for a 90 day period. Both bone-nHA and Syn nHA were encapsulated with commercial DAP and NPK fertilizers. The techniques SEM, XRD, and FTIR were employed to characterize the nanofertilizers, while AAS was used to determine levels of Cd and Pb, and UV measured NO3- and PO43-levels. The bone nHA was less coagulated with significantly smaller diameter compared to Syn nHA (P˂0.05). Further, bone-nHA significantly reduced Cd (range 58 – 89 %) and Pb (range 62 - 91 %) uptake and had higher adsorption of the metals (P˂0.05). Growth performance parameters for the crops grown with bone-nHA improved by over 56 %, being better than those grown with the Syn nHA and it is encapsulated nanofertilizers (P˂0.01). Results support presence of higher number of adsorption sites in the bone-nHA implying a better performance as a nanofertilizer. At 40 days bone nHA had significantly higher nitrate release rate of 28 % in comparison with syn nHA (P˂0.01). Adsorption equilibrium data fitted well with Langmuir for Cd while Pb fitted well with Freundlich isotherm. Bone nHA nanofertilizers are recommended to reducing Cd and Pb uptake and adsorption, improving growth performance and nutrient release on growing beans (P. Vulgaris L.), spinach (Spinacia oleracea) and kales (Brassica oleracea acephala).

# CHAPTER ONE

# INTRODUCTION

## 1.1 Background Information

The world’s population continues to grow, and is projected to reach 8.0 billion by the year 2030 (FAO, 2015). This global population increase, and in addition to rapid urbanization and limited agricultural land leaves agronomists with a challenge to feed the population. The human settlement in rural and urban areas is as a result attributed to the decrease in agricultural land (Rameshaiah et al., 2015). Furthermore, satellite images reveal a reduction of fertile land due to leaching and eutrophication of macro and micro-nutrients like, nitrates (NO3-), phosphates (PO43-) and potassium (K+) due to excessive use of commercial fertilizers (Willer and Lernoud, 2015; Nilwala et al., 2011). Indeed the threats in food production have lead farmers into over-cropping, continuous tillage, growing of fast-maturing crop varieties and top dressing (El-Feky et al., 2013; Kole et al., 2013). Mostly, these practices deplete soil nutrients hence calling for the excessive application of commercial fertilizers (Srivastava et al., 2014; Prasad et al., 2012). The fore mentioned practices are experienced in the study area, Kisii County, Kenya.

The over-application of commercial fertilizer (DAP, NPK) on crops faces the challenge of nutrient leaching which makes nutrients not only unavailable but also limits their interaction to the plant, hence lowering crop yields (Das et al., 2016). The over-application of commercial fertilizers also alters soil physico-chemical properties like electrical conductivity (EC); soil pH, and % organic matter (% OM), (Srivastava et al., 2014; DeRosa et al., 2010). Low soil pH for example increases the mobility of nutrients hence leaching them to lower soil levels that would not be available for plant uptake (Zhou et al., 2019; Song et al., 2013). As a result there is increased uptake of cadmium (Cd) and lead (Pb) which are among most toxic heavy metals (Buyukkilic et al., 2022; Guangmei et al., 2021). Heavy metals on one hand threaten food safety while on the other, their exposure to human beings damages the functioning of the central nervous system, lungs, kidneys, liver, and may cause cancer (Rezvani et al., 2012).

The synthesis and use of nanoparticle materials in the agricultural sector has partially contributed to increasing food production as a solution to the prevailing challenges earlier mentioned (Tarafdar et al., 2014; Song et al., 2013). Nanotechnology consist designing, producing, characterizing, and application of particles by regulating their shape and size to nanometer scale (Helaly et al., 2014; Kole et al., 2013). Numerous adsorption sites and selective adsorption towards some metal ion is a unique feature of nanoparticles that make it attractive. Hence they are essential in the development of slow and sustainable release of nutrients, pesticides and herbicides. As such, nanotechnology techniques are essential in promoting the use of environmentally friendly and sustainable agricultural inputs (Raliya et al., 2015; Prasad et al., 2012). Nanohydroxyapatites (nHA) is an example to such nanoparticles which are synthesized from hydroxyapatites [Ca10(PO4)6(Z)2, Z = F, Cl, OH]. They are non-toxic and have higher selective adsorption to heavy metals, that’s why they were used in Nyakoe greenhouse study (Suchanek et al., 2019).

According to Nilwala et al. (2011), hydroxyapatite is inorganic phosphate rock and is a vital source of phosphorus (P) in fertilizer. The synthesis of synthetic nanohydroxyapatite is challenging since phosphoric acid and calcium hydroxide used in synthesis are expensive. This study envisaged that the use of bones nHA would offer a preferred cheaper option. There are millions of tones of bones in dumping sites which pose an environmental pollution menace due to their long period to biodegrade (Suchanek et al., 2019). It was envisaged that the bones provide an option for the synthesis of bone nHA nanoparticles. It also bears the advantage of being non-toxic, and has higher selective adsorption to heavy metals (Suchanek et al., 2019; Zhangwei et al., 2019). The application of synthetic nHA nano fertilizers has improved the performance of crops such as maize (Suchanek et al., 2019; Raliya et al., 2015).

Nanoparticles can be coated with commercial fertilizer to enable them to control the release of plant nutrients to the crop (Zhang et al., 2019). Studies shows that, the application of commercial nitrogenous, phosphatic, and potassium fertilizers and micronutrients using nanoparticles increases the nutrient use efficiency in grain crops (Zhang et al., 2019; Ma et al., 2013). Ma et al. (2013) reported that the use of nano-doped fertilizers increases crop productivity. Among the methods of preparing nHA crystals are wet chemical precipitation, sol-gel, biomimetic deposition, and electro-deposition (Wang et al., 2016). The wet chemical precipitation method was employed in this study to synthesize nHA nanoparticles. These synthetic nHA have been used for growing several crops including cereals, vegetables, and legumes (Sun et al., 2020; Muhammad et al., 2019; Disfani et al., 2017).

At maturity, vegetables and legumes such as beans and soybeans have shown higher uptake of Cd, Pb and Mn heavy metals especially when grown in highly polluted soils, they uptake heavy metals beyond FAO/WHO permissible levels of 10 µgg-1 (Wang et al., 2016). The major source of these heavy metals in Kisii County is sewage effluents used in watering of vegetables. The levels of heavy metal uptake by crops depends on the level of plant maturity especially within 30 to 90 days, with some studies showing reduction of heavy metal uptake with plant maturity due to their immobilization by nanoparticles (Mohammad et al., 2019; Sezgin et al., 2019). However at maturity, heavy metals levels in crops should not go beyond FAO/WHO permissible levels of 10 µgg-1. Nanoparticles such as synthetic nHA have been used to lower heavy metal uptake and improve crop growth parameter majorly plant height (Zhangwei et al., 2019; Raliya et al., 2015). It can also improve other growth parameters namely, dry weight, leaf diameter, number of leaves and tillers, stem diameter, number of pods, crop yield, leaf surface area and chlorophyll content (Du et al., 2019; Dwivedi et al., 2016).

Notably, synthetic hydroxyapatite has been used to improve soy bean dry weight performance by 75 % (Zhangwei et al., 2019). Similarly other researchers have used synthetic hydroxyapatite nanoparticles to increase dry weight in soy bean by 20 % (Liu and Lal, 2014). The use of bone nHA was investigated on common bean (P. Vulgaris L.), spinach (Spinacia oleracea) and kales (Brassica oleracea acephala), commonly known as sukuma wiki which are food crops commonly consumed in Kisii County. Bones are generally inexpensive, non-toxic and highly selective (Suchanek et al., 2019). The common bean belongs to the legume family (Fabaceae) and is among the oldest and most common legume crops grown in East Africa (Pramod et al., 2013) and in Kenya. The kales and spinach are both heavy metal accumulators, however both of them were chosen in this study because they vary in their level of heavy accumulation.

The thermodynamics working principle of nanoparticles to guarantee higher and sustainable crop growth is due to a negative change in Gibb’s free energy. When nanoparticles are encapsulated with fertilizers (nano fertilizers), their higher entropy makes the change in Gibbs free energy to be negative. This makes the reaction spontaneous and faster in the forward direction that guarantees the slower and effective release of crop nutrients (Song et al., 2013; Bertazzo et al., 2010). The nanoparticle thermodynamic adsorption capacity of Cd and Pb was investigated using linearised Langmuir and Freundlich isotherms. The efficacy of nano fertilizer adsorbents was evaluated and quantified by pseudo first-order and pseudo second-order kinetic models. The nanoparticle functional groups were investigated by Fourier Transform Infra-Red (FTIR), while nanoparticle morphology and particulate size were measured by Scanning Electron Microscopy (SEM) and X-Ray Diffraction (XRD) respectively. At maturity (60-90 days) Cd and Pb concentration levels in kale, spinach, bean plant, and isolated fraction was investigated since they are being priority toxic heavy metals were done by Atomic Absorption Spectroscopy (AAS). Nutrient release rate batch experiment was done by Ultra Violet spectroscopy (UV).

## 1.2 Statement of the Problem and Justification

Rapid population growth that is currently at 7.2 billion people poses the threat of hunger and acute food shortage especially in developing countries where already millions of persons suffer from hunger (FAO, 2015). This threat is attributed to the limited agricultural fields which are decreasing as a result of human settlement and industrialization. Therefore, this has called for use of commercial fertilizer on the limited land space to increase food production. However, over application of commercial fertilizers reduces soil pH and % soil organic matter hence increasing uptake of Cd and Pb (Willer and Lernoud, 2015; Konate et al., 2014).

Based on the challenge of using commercial fertilizers, alternative methods to increase food production have been explored. These include the use of synthesized nanoparticles to make nano fertilizers from carbon nano-tubes, calcites, gypsum, apatites, metal oxide particles, activated carbon, hydroxyapatites and the now proposed use of bone nHA. Nano fertilizers have many adsorption sites that ensure the slower release of nutrients such as NO3-, PO43- and K+ to guarantee their longer interaction with plants thereby increasing crop yields. Furthermore, they immobilize Cd and Pb heavy metals, eventually reducing their uptake in crops (Gil-Díaz et al., 2017).

Bone nHA is envisaged to portray an advantage over other nanofertilizers, since they contain essential crop nutrients such as phosphorus and calcium (Suchanek et al., 2019). Globally, 130 billion kilograms of bones are dumped annually from slaughterhouses with 3 billion kilograms recorded in Kenya alone, which is essentially an environmental menace (Suchanek et al., 2019). Using Bone in this study not only presents readily available material for synthesis of nano-fertilizers for increased food production but also reduces environmental pollution. In order to address the potential contribution of bone nanofertilizers in food production which has not been investigated, the growth performance parameters namely plant height , leaf diameter, number of leaves and stem diameter of spinach, sukuma wiki, and beans were studied with the application of the nano fertilizers. Further, the findings on the effects on regulating the nutrient release rate of NO3-, PO43- and K+ and the heavy metal (Cd and Pb) adsorption kinetics will provide information on the effectiveness of the bone nano fertilizers.

## 1.3 Null Hypotheses

There is no effect on the use of bone nHA and synthetic nHA hydroxyapatite nano-fertilizers on adsorption and uptake of cadmium and lead, nutrient release and growth performance on selected crops.

## 1.4 Objectives

### 1.4.1 General Objective

To investigate effect on the use of bone nHA and synthetic nHA hydroxyapatite nano-fertilizers on adsorption and uptake of cadmium and lead, nutrient release and growth performance on selected crops.

### 1.4.2 Specific Objectives

- To characterize synthesized and encapsulated bone nHA nano-fertilizers with NPK, DAP encapsulations using SEM, XRD and FTIR analysis.

- To determine the uptake levels of cadmium and lead in bean (P. Vulgaris L.), spinach (Spinacia oleracea) and kales (Brassica oleracea acephala) leaves grown for 90 days in a greenhouse using bone nHA nano-fertilizers with NPK, DAP encapsulations.

- To determine the growth performance of bean (P. Vulgaris L.), spinach (Spinacia oleracea) and kales (Brassica oleracea acephala) grown for 90 days using bone nHA nano-fertilizers with NPK, DAP encapsulations.

- To assess the 24 hour efficiency of Cd and Pb adsorption by bone nano-fertilizers using Langmuir, Frendlich isotherms and kinetic models batch experiment.

- To assess the 40 day efficiency of NO3-, PO43- and K+ nutrients release levels by bone nHA nano-fertilizers using batch experiment.

## 1.5 Significance of the Study

Results show the effect of hydroxyapatite nano fertilizer synthesized from synthetic and bones on the plant height, number of leaves, leaf diameter and stem diameter on kale, beans, and spinach. Further the findings show the potential of bone nHA to immobilize heavy metals Cd and Pb which is a good attribute for food safety. Suchanek et al. (2019) noted that bones have low biogradability in dumping sites. Hence, use of bone nano fertilizers will also solve the environmental effects of bone dumping as waste and by extension job creation is foreseen for those collecting the bones. Buyukkilic et al., 2022 noted that 70 % of food production relies on commercial fertilizers yet they have negative effects and are expensive. Therefore, bone nanofertilizer can serve about 40 % of phosphatic fertilizer need by farmers in Kenya to reduce on over reliance on commercial fertilizers.

## 1.6 Scope and Limitation

In the array of inorganic and organic analytes, the heavy metals Cd and Pb and nutrients NO3-, PO43-, and K+ were studied, being priority toxic heavy metals and essential nutrients respectively. Any characteristic of the bones including the type or source, which would determine their performance, was not considered in the synthesis of the bone nHA. The study narrowed to carrying out the study using sand loamy soil. Plant growth and nutrient uptake differs among plants. In this study plant height, leaf diameter, number of leaves, number of pods and stem diameter were considered as the growth parameters. The uptake levels of Cd and Pb and growth parameters were investigated on one legume (P. Vulgaris L.) and two vegetable crops, spinach (Spinacia oleracea) and kales (Brassica oleracea acephala) grown within their maturity period of 30-90 days.

# CHAPTER TWO

# LITERATURE REVIEW

## 2.1 Commercial Fertilizers in Crop Production

Food insecurity is a global concern in the wake of an ever-ballooning population, which is expected to reach over 8 billion between the years 2030 and 2050 (FAO, 2015). The concern is greater in developing countries for example in Kenya where about 32 % of her population is affected especially those in arid and semi-arid counties (FAO, 2015; Willer and Lernoud, 2015). One common approach to address the concern is the use of commercial fertilizers, and it is deduced that 30 % of crop production is as a result of their use. Other approaches include the growing of high-yielding crops, growing of fast-maturing and fertilizer responsive crops (El-Feky et al., 2013). However, due to scarce fertile arable land, this leads to over tillage of food crops hence depleting soil nutrients, leading to poor yields which may require alternative fertilizers.

Intensive farming practices are attributed to account 40 % of land degradation, leading to a severe loss of soil nutrients (Srivastava et al., 2014; Prasad et al., 2012; Nilwala et al., 2011). The deficiency of macronutrients like NO3-, PO43- and K+ in crops not only affects the crop productivity but also human health by consumption of foods deficient of essential micronutrient. For example, phosphorus deficiency in consumed food causes human growth impairment, weak bones, and decreased cognitive performance in humans (Kole et al., 2013).

The major shortcomings of over reliance on use of commercial fertilizer include leaching and reaction with soil moisture (for fertilizer like urea) to form ammonium carbonate. While the former makes nutrients unavailable to crop roots, the latter can cause loss of the nutrient to the atmosphere in form of ammonia gas (Das et al., 2016; Cai et al., 2014). The loss of nitrates due to draining out of urea nutrients much deeper in the soil which is out of reach to the plant roots contributes to 90 % of nutrient loss (Das et al., 2016). This has called for nano-technological strategies in nano-fertilizer manufacturing for slower and gradual release of nutrient, pesticides and herbicides (Ahmed, 2018, Cui et al., 2010). Thus nanotechnology is vital in development and promoting the use of environmentally friendly and sustainable agricultural inputs (Raliya et al., 2015; Prasad et al., 2012).

## 2.2 Nano-fertilizers

Nano-fertilizer is a substance that uses nanotechnology to incorporate nutrients in nanoparticles to regulate rate of nutrient release to plants (Davarpanah et al., 2016; Ma et al., 2013). Nanoparticles can be made from adsorbents like zeolites, cow manure, apatites, and hydroxyapatites that have been developed in recent studies to immobilize Cd and Pb (Ngorwe et al., 2014; Nilwala et al., 2011). In addition, zeolites nanoparticles have been used for the controlled release of growth enhancers. Ma et al. (2013) showed that the use of nitrogenous, potassium and phosphatic nano-fertilizers, in grain crops increases micronutrients and amino acids uptake and regulates the NO3-, PO43-release rate.

The unique properties of nanoparticles like increased number of adsorption sites and selective adsorption of some essential substances has been found essential for slower and controlled delivery of drugs to patients (Giroto et al., 2015) and nutrients (Konate et al., 2014) to crops in the fields of medicine and agriculture respectively. Nanoparticles made from bone have been found to have more stable adsorption sites than synthetic nanoparticles of hydroxyapatites made by chemical precipitation. Hence in the agricultural sector; bone nHA are likely to have more gradual release of nutrients to crop (Tarafdar et al., 2014).

Commercial fertilizer encapsulation within the nanoparticle has been invented in nanotechnology and can be done in three methods (Suchanek et al., 2019; Ma et al., 2013). Firstly, is through nutrient encapsulation inside a nano-porous material for a more controlled release to the crop. In a study by Ma et al., 2013, urea encapsulated in carbon nano-tubes was used to improve maize seed yield by 31.2 %. Secondly, coating nanoparticles with nutrient enriched thin polymer film to guarantee gradual and sustainable release of nutrients to crops (Suchanek et al., 2019). Thirdly, spraying commercial fertilizer in form of particles or emulsions to nanoparticles to form nano-fertilizers thereby regulate the nutrient release. Therefore nitrates (NO3-), and phosphates (PO43-) release and eventual uptake by the plants is regulated, thereby preventing undesirable nutrient lose pathways like soil, water, air and weeds (Giraldo et al., 2014; Ma et al., 2013; DeRosa et al., 2010).

## 2.3 Effects of Nano fertilizer on Cd and Pb Uptake

For decades adsorbents have been used to immobilize some heavy metals like Cd and Pb to minimize their eventual uptake in plants (Rizwan et al., 2017; Musico et al., 2013). Among the inorganic adsorbents that have been used to immobilize Cd include, rock salt, apatite, biochar, hydroxyapatite (HA), zinc oxide, iron (III) oxide and manganese (IV) oxide (Sun et al., 2020; Zahra et al., 2019; Zhangwei et al., 2019). Research by Sun et al. (2020), explored biochar nanoparticles in Cd2+ adsorption, whereby efficiency of the biochar increased due to nanoparticle having larger exposed surface area to volume ratio. Zahra et al. (2019) investigated reduction of Cd uptake in wheat using ZnO nanoparticles with the results indicating Cd uptake reduced by 80.1 % while Zhangwei et al. (2019) used synthetic nHA nanoparticles to reduce Pb2+ uptake in soy bean by 58.1 %.

The efficiency of SiO2 nanoparticles to reduce Cd in Pennisetum Species (Dong et al. (2019)) and wheat (Naeem et al. (2018)) have already been investigated. The study by Dong et al. (2019) varied nanoparticle dosage so that SiO2 nanoparticles reduced Cd in Pennisetum Species by 23 to 37 %. The Cd heavy metal also was reduced by 28 % in wheat when the SiO2 nanoparticles were applied (Naeem et al., 2018). Other nanoparticles including ZnO, zinc–lysine nanoparticle and nano-Fe3O4 have also been employed in immobilizing Cd hence reducing its uptake in various plant parts to improve their growth (Rizwan et al., 2019; Zhou et al., 2019; Saifullah et al., 2016). When ZnO nanoparticles were employed, Cd decreased in wheat grain (Saifullah et al. (2016)) and in the wheat shoot (Zhou et al. (2019)) by 74 % and 17 % respectively. Rizwan et al. (2017) added the zinc–lysine nanoparticles which reduced Cd levels in green pepper and eggplant fruits by 11.5 % and 15.4 % respectively. Varying the percentage of the adsorbent dosage has shown a directly proportional decrease in Cd levels (Abbas et al., 2017). Abbas et al. (2017) while working with biochar nanoparticles noted that varying nano-biochar from 1.5 % to 5 % resulted in Cd uptake reduction from 26 % to 57 %, in wheat grain. This implies that various nanoparticles dosage have an effect in immobilizing Cd, thereby reducing its uptake in crops. The efficiency of these nanoparticles to immobilize heavy metals depends on the dosage of the nanoparticles applied. Similarly, nanoparticles such as synthetic nHA have been applied to lower Pb uptake in several plants. Zhangwei et al. (2019) showed that, the addition 30 g⋅kg−1synthetic nHA in heavy metal polluted soil reduced Pb in soy bean by 58.1 % (shoot) and 53.0 % (roots). This study investigated use of bone nHA nano-fertilizer in growing kales, spinach and beans in Cd/Pb medially polluted soils to reduce uptake to FAO/WHO permissible levels of 10 µgg-1 at maturity of the 90th day (Sezgin et al., 2019; Wang et al., 2016).

In addition, other than reduction of Cd and Pb uptake by nanoparticles, other heavy metals have also been immobilized by use of the nanoparticles. The findings by Alexandre et al. (2017) showed that nano-Fe3O4 reduced Zn and Cu in wheat seedling by 11.39 % and 52.94 % (shoot), respectively. Other nanoparticles including ZnO, zinc–lysine nanoparticle and nano-Fe3O4 have also been employed in immobilizing Zn hence reducing its uptake by crops (Du et al., 2019; Zhou et al., 2019; Rizwan et al., 2017).

## 2.4 Hydroxyapatite Nano fertilizers and their Heavy Metal Immobilization in Plants

Hydroxyapatite (HA) is a vital inorganic phosphate rock material that resembles the bone in terms of chemical and structural composition. This apatite group has the formula [Ca10(PO4)6(Z)2, Z = F, Cl, OH], structural site Z is commonly occupied by OH. This biomaterial is used for replacement and repair of bone or teeth. Chemical precipitation, sol-gel, biomimetic deposition, bone milling, and electro-deposition are some of the methods of preparing synthetic nanohydroxyapatite (syn nHA) that have been developed (Suchanek et al., 2019; Bertazzo et al., 2010). Bones contain essential plant nutrients like phosphorus and calcium which are critical for good food quality and better growth performance in plants (Suchanek et al., 2019; Liu & Lal, 2014). Notably, millions of tones of bones are available in litter dumping sites and because they take longer to biodegrade, they cause an environmental pollution menace. They would hence provide cheap and most effective source of bone nHA when synthesized to nanoparticles.

The plant uptake of Cd and Pb heavy metal can be minimized through application of various soil adsorbents since these immobilize them and lower their uptake in crops (Rizwan et al., 2017; Lee et al., 2012). Among the factors that would determine the levels of metal uptake by plants is their maturity and it has been shown that as the plants mature the heavy metal uptake levels reduces (Mohammad et al., 2019). Another factor is the nanoparticles dosage applied, as well as the plant part analyzed (Dong et al., 2019; Zhangwei et al., 2019).

These properties of nanoparticles have been explored to develop nano fertilizers with higher adsorption capacity, selectivity and non-toxic (Muhammad et al., 2019; Yaoyao et al., 2019; Ling et al., 2017). Among these properties is the efficiency of the nano-adsorbent material to immobilize heavy metal, which is directly proportional to surface area of the nanoparticles exposed (Sun et al., 2020).

The HA nanoparticles (Ca10(PO4)6(OH)2) thus continue to be explored as a potential alternative phosphatic fertilizer (Liu & Lal, 2014) and for immobilization of heavy metals (Wang et al., 2016; Konate et al., 2013). As a result of the latter, they not only reduce the heavy metal uptake by vegetables but enhance their growth indicators like height, number of leaves and pods, leaf diameter and stem diameter (Zhang et al. 2019; Dwivedi et al., 2016; Raliya et al., 2015; Prasad et al., 2012). Bone nanofertilizers have added advantage of being non-toxic. The study was conducted in Nyakoe Kisii county using artificial medially Cd/Pb polluted sandy loamy soils. Human exposure to Cd and Pb heavy metal is mainly through ingestion of contaminated food, although exposure can also be through water, air, or skin absorption (Zhu et al., 2019; Rezvani et al., 2012). Absorption of heavy metals in kales, spinach, and beans may hence be inevitable since vegetables are grown in polluted soils (Muhammad et al., 2019). Their dangers cannot be underscored, and in particular, effects of long-term exposure to Cd and Pb include cancer, Parkinson’s disease, muscular dystrophy, sudden infant death syndrome (SIDs), multiple sclerosis, and neurological degenerative processes like mimic Alzheimer’s disease (Davarpanah et al., 2016; Helaly et al., 2014). The effects of Cd and Pb toxicity in plants include stunted growth, wilting, chlorosis and necrosis (Musico et al., 2013).

As already stated, studies on the HA nanoparticles indicated that they immobilize heavy metals in plants (Zahra et al., 2019; Zhangwei et al., 2019; Wang et al., 2016). In both studies by Zahra et al. (2019) and Zhangwei et al. (2019) the efficiency of HA nanoparticles to immobilize heavy metals is supported. The former study investigated reduction of Cd uptake in wheat using ZnO nanoparticles and results indicated Cd uptake reduced by 80.1 % while in the later, a 58.1. % decrease in Pb2+in soy bean was reported. Similar observations had earlier been made by Wang et al.(2016) where silicon oxide-based nanoparticle treatment resulted in a decrease in Pb uptake by 59.25 % while commercial fertilizers increased Pb in kale by 14 % in comparison to 0 % of the control. However, most studies have not embraced use of nHA nano-fertilizers especially bone nHA, which is locally and cheaply synthesized and its non-toxic in growing kales, beans and spinach to reduce heavy metal uptake and enhance growth performance in these vegetables. This is what was embarked in this study.

## 2.5 Effect of Nano fertilizers on Plant Growth Performance

Growth performance is the change of growth performance parameters like height, leaf diameter, number of leaves and tillers, stem diameter, plant dry weight, and crop yield (Raliya et al., 2015). Nanoparticles have been used not only to reduce heavy metal uptake, but also in improving crop growth performance on the number of leaves, height, leaf diameter, number of pods, and stem diameter as major growth indicators (Shojaei et al., 2019; Dubey et al., 2016; Shalaby et al., 2016). The nanoparticles have improved growth performance; the mostly used growth parameter is plant height, which can be measured in 30, 60 and 90 day intervals. Other growth parameters that can measure growth performance include stem diameter, number of leaves, leaf diameter, number of pods, and crop dry weight which can be measured at maturity (Melika et al., 2015; Liu & Lal, 2014). Further, they ensure higher nutrient use efficiency and have regulated nutrient release rate (Mehrazar et al., 2015; Cai et al., 2014). Some underlying factors that can be attributed to crop growth parameters are monitored while administering the nHA include the age of the plant, part of the plant, species of the plant and dosage of the fertilizer (Mohammad et al., 2019).

In particular, Ag-oxide, Cu-oxide, FeO, TiO2, ZnO, and hydroxyapatite nanoparticles, have been found to increase crop growth in mung bean, soybean, spinach, peanut, onion, wheat, tomato, mustard and potato (Iqbal et al., 2019; Davarpanah et al., 2016). Iqbal et al. (2019) used Ag2O nanoparticles to increase wheat height by 36.2 % while Davarpanah et al. (2016) used ZnO nanoparticles to increase dry weight biomass by 29.2 %.

In exploring effect of Fe/SiO2 nano-fertilizers on plant growth, an amount of 15 mg kg-1 increased height of maize and barley seedlings by 20.8 %, and 8.25 %, respectively (Disfani et al., 2017). Dry weight was also reported to increase when NPK encapsulated carbon nanoparticles were used by various studies. The increases recorded were for maize (10.93 %) (Melika et al., 2015), vegetables (12.34 %) (Prasad et al., 2012), rice (19.76 %) (Muhammad et al., 2019), soybean (19.74 %) and wheat (28.81 %) (Muhammad et al., 2019), and passion fruit (128 %) (Giraldo et al., 2014). Pramod et al. (2013) used ZnO nanofertilizers to enhance barley dry weight by 62 %. Similarly, synthetic hydroxyapatite nanoparticles have been used to increase dry weight in soy bean by 75.5 % (Zhangwei et al., 2019), soy bean by 20 % (Liu and Lal, 2014). On the other hand, Yuvakkumar et al. (2011) used SiO2 nano fertilizers as a foliar spray to enhance number of leaves and increase maize yield by 600 Kg/Ha. The increase in growth performance is attributed to gradual release of nutrients to the plant when required (Mohammed et al., 2019; Song et al., 2013).

Studies by Raliya et al. (2015), titanium (IV) oxide nanoparticles were used to increase the growth of mung bean (Vigra radiate L.) by bio fertilization. Carbon nanoparticles encapsulated with fertilizer were found to increase dry weight of soybean by 12.12 % in comparison with the control (Prasad et al., 2012). Sun and co-researchers using biochar nanoparticles also reported an increase of 10.69 % of dry weight biomass and 51.5 % in leaves number in comparison with the control (Sun et al., 2020). Zhang et al. (2019) noted that the application of TiO2 at a 2.5 % (w/w) level was reported to increase dry weight biomass in spinach by 3.13 %.

This implies that the use of nanoparticles is essential in agricultural revolution to increase food quality and quantity to feed the sporadic growing population. This is in support of fact that the nanoparticles have more enhanced number of adsorption sites that provides larger exposed surface area to volume ratio for higher immobilization of toxic heavy metals and more controlled nutrient release to the crops when needed, thereby increasing growth performance and safety as reported above by various researchers. However most of the reported nanoparticles above that have shown to play such a key role in food production are too expensive to synthesize, thereby increasing cost of food production. This study used bone nanoparticles and its encapsulation to check of Cd and Pb uptake and growth performance in kales, spinach and beans. This is because bone nanoparticles are non-toxic, have stable adsorption sites and are cheaply available.

## 2.6 Nano-fertilizer Thermodynamics

The thermo dynamic concepts of nanofertilizers are anchored on the 2nd law of thermodynamics, which states that the entropy (S) of the particles is linearly proportional to the randomness of its system. Nanoparticles have more particulates per unit volume compared to ordinary commercial fertilizers; hence they have higher entropy which is linearly proportional to Gibb's free energy. Nanoparticles have higher Gibb’s free energy (G) which increases its kinetic energy to hasten particulate movement (Hameed et al., 2017; Bertazzo et al., 2010). This increases nanoparticles mobility across the experimental soil structure surrounding the plant. This explains why there is more controlled release of nutrients by the nano-fertilizers in comparison with commercial fertilizers. Change in Gibbs free energy is given by Equation 2.1;

ΔG = ΔH – TΔS                                                                           (2.1)

ΔG = Gibb’s free energy change

ΔH = Enthalpy change of the reaction

ΔS= Entropy change of the reaction

T= Temperature of the reaction

When entropy of experimental soil increases, then ΔG is more negative, implying that the reaction is spontaneous and the forward process is favored (Prasad et al., 2012; Wu et al., 2012). Hence when nHA nanoparticles are encapsulated with commercial fertilizers to make nanofertilizers, their higher entropy makes the ΔG to be negative making the adsorption reaction spontaneous and faster in the forward direction that guarantees the gradual and effective release of plant nutrients (Shojaei et al., 2019; Montanzeri et al., 2010). Therefore the negative change in Gibbs free energy increase the rate of penetration of nano-fertilizers inside the experimental soil structure (Dubey et al., 2016; Cai et al., 2014; Nilwala et al., 2011).

## 2.7 Effects of Experimental Conditions on Adsorption of Cd and Pb

The efficiency of nano-fertilizers is strongly influenced by the effect of initial pH of media, adsorbent dosage, initial heavy metal ion concentration and contact time (Shojaei et al., 2019; Wu et al., 2012).

### 2.7.1 Effect of Soil pH on Adsorption of Cd and Pb

The adsorption process of metal ions is controlled by the soil pH which is attributed to its effects on metal ions solubility and the concentration of the counter ions on the nanoparticle surface (Montazeri et al., 2010). Low soil pH controls the protonation process of the nanoparticle surface by H+ ions competing with Cd2+ and Pb2+ metal ions in the adsorption sites making the metal adsorption lower (Banerjee et al., 2019; Das et al., 2012). The nanoparticle surface becomes more positively charged thus causing repulsion between the nanoparticle surface and the positively charged metal ions (Liu & Lal, 2014). Thereby the heavy metal mobility increases at extremely higher acidic conditions, thus increasing its bioavailability for uptake by crops. The adsorption is lowest at pH 2 and increases linearly as pH increases up to optimal pH of 6, (Das et al., 2016). The pH 5-7 has been reported for optimum Cd adsorption by nanoparticles (Wang et al., 2016). Additionally Qi et al. (2020) used nano-zeolite clay to establish maximum adsorption of Pb at pH 6.

### 2.7.2 Effect of Adsorbent Dosage on Adsorption of Cd and Pb

The amount of adsorbent dosage affects the adsorption process. The higher the adsorbent dosage, the higher the adsorptive capacity which is attributed to the increase in number of adsorption sites on the exposed adsorbent surface area (Singh et al., 2018). However at very high adsorbent dosage the adsorption process declines due to partial aggregation of the adsorbent causing overlapping of active adsorption sites (Piao et al., 2012). This is supported by research done by Hameed et al. (2017), that established that zinc (Zn) adsorption was highest at 99.22 % (dosage 3.5 g/L), 95 % (dosage 4.0 g/L), 98 % (dosage 3.0 g/L), 89 % (dosage 2.5 g/L) and  86 % (dosage 2.0 g/L)) using carbon nano-tubes. On the other hand, it was 93 % (dosage 3.0 g/L), 86 % (dosage 2.5 g/L), 85 % (dosage 2.0 g/L) and 79 % (dosage 1.5 g/L), for removal of lead using carbon nano-tubes (Hameed et al., 2017).

### 2.7.3 Effect of Contact Time on Adsorption of Cd and Pb

Adsorbent efficiency is measured in correlation with the contact time of adsorbate and adsorbent, but the shorter the adsorption time, the higher the efficacy of the adsorbent (Lateef et al., 2016). Therefore, controlling the residence time for metal ions adsorption on the adsorbent surface determines the rate of metal ion uptake and metal ion activity on adsorbent surface (Ling et al., 2017; Bertazzo et al., 2010). When adsorption reaches the point at which the amount of ions adsorbing is equal to amount being desorbed the process is said to be in a state of dynamic equilibrium (Tarafder et al., 2020).

Studies using carbon nano-tubes reported copper removal of 64 % in 30 minutes 84 % in 80 minutes (Banerjee et al., 2019). Whereas Piao et al., (2012) reported that contact time of 30 minutes attained 71.47 % adsorption of copper and 120 minutes for a 99.9% removal of lead. Equilibrium time for Cu2+ and Pb2+on ZnO nanoparticles was achieved within 120 minutes with 94 % and 100 % removal respectively (Calin et al., 2012). Similarly, other studies achieved equilibrium time of 120 minutes reporting in carbon nano-tubes for cadmium (Janan et al., 2014). Therefore, from these studies, 2 hours is optimal time for maximum adsorption of heavy metals from aqueous ions of their solutions, explaining why this 2 hours contact time was used in this study.

### 2.7.4 Effect of Initial Metal Ion Concentration on Adsorption of Cd and Pb

Initial metal ion concentration has a strong influence on the adsorption process (Montazeri et al., 2010), which is normally carried out at optimized conditions of adsorbent dosage, contact time and experimental pH by varying the metal ion concentration (Montanzeri et al., 2010). At lower metal concentrations, the adsorption process is favorable. However, at increased metal ion concentrations, the adsorption efficiency decreases due to reduction of number of adsorption sites in relation with increasing metal concentration (Calin et al., 2012). Study on Zn adsorption using carbon nano-tubes reported the removal efficiencies of 97 % in 10 ug/ml., 98 % in 7 ug/ml. and 99 % in 5 ug/ml (Banerjee et al., 2019).

### 2.7.5 Adsorption Isotherms

Adsorption is a physical or chemical process involving interactions between the surface of adsorbent and metal ions. Adsorption is accumulation of particles to form a thin film on the adsorbent surface. The Langmuir isotherm is applied to monolayer adsorption on homogenous sites. Physicochemical parameters such as substance pH and electrical conductivity (EC) influence adsorption. The linear form of Langmuir isotherm for Cd and Pb adsorption can be represented by Equation (2.2) shown below (Wang et al., 2016).

1qe=1cqmax+1b                                                                                                      (2.2)

Where; b represents Langmuir binding energy, qmax (mg.kg-1) is the maximum adsorptive capacity of adsorbent, c (mg.dm-1) is the concentration of the left adsorbate experimental solution at equilibrium,1 qe is the quantity of metal ion adsorbed per unit weight of nanoparticles. The Langmuir isotherm parameters are obtained by plotting linear graph of 1qeagainst  1c. If the data is linear, then the Langmuir isotherm model is appropriately fitted with correlation coefficient R2 close to 1. Using the linear plot, the term qmax (reciprocal of the slope) and parameter b (reciprocal of the Y-intercept) can be found (Piao et al., 2012; Wu et al., 2012). The Freundlich isotherm is applied to multilayered adsorption on heterogeneous sites. Similarly, the adsorption capacity of Cd and Pb using bone nanofertilizers can be fitted in the Freundlich isotherm model given in Equation (2.3), which is expressed as:

qe=Kc1/n                                                                                                              (2.3)

Where qe is the quantity of metal ion adsorbed per unit weight of nanoparticles, c is the metal ion concentration left at equilibrium; Kf and n are constants representing the adsorptive capacity and binding energy respectively (Banerjee et al., 2019; Hameed et al., 2017).

The Freundlich linear plot of log qe against log c is plotted, where constant n and qmax are obtained as antilog of reciprocal of gradient and antilog of Y- intercept respectively. Constant n is a measure of the deviation of adsorption process from linearity (Chuanjia et al., 2015). If n˃1 for the adsorption on synthetic nHA and bone nHA samples, it is a physical process. When the obtained 1/n˂1, it shows adsorption is heterogeneous and a linear Freundlich isotherm (Shojaei et al., 2019; Zahra et al., 2019). The best-fitted model picking is anchored on the determination of the correlation coefficient R2. The nearer R2 value is to unit (1) between the Langmuir isotherm model and the Freundlich model, the better the adsorption model (Zhangwei et al., 2019; Wu et al., 2012).

### 2.7.6 Adsorption Kinetics

This study estimated the order and rate constant of the adsorption process applying the pseudo 1st order kinetic and pseudo 2nd order kinetic models. The pseudo 1st order kinetic model is given by Equation 2.4 (Hameed et al., 2017).

logqe-qt=logqe-k12.303t……………………………….2.4

Where qe(mg.g-1) is the adsorptive capacity at equilibrium and qt (mg.g-1) is the adsorptive capacity at time of t (min), k1(min-1) is the pseudo 1st order rate constant of adsorption. The constants k1and qewere computed from a plot of log (qe-qt) versus t as natural antilog of gradient and antilog of y-intercept in that order. The pseudo 2nd order kinetic model is expressed by Equation 2.5 (Banerjee et al., 2019).

tqt=1k2.qe2+1qet……………………………………2.5

Where k2(g/mg·min) is the rate constant of pseudo-second order adsorption process. The constants qeand k2were worked from a plot of tqt versus t. as reciprocal of gradient and Y-intercept divide by qe2 respectively.

## 2.8 Analytical Methods

The atomic absorption spectroscopy (AAS) has been used for determination of several heavy metals including Cd and Pb (Asare et al., 2019) whiles the techniques UV-visible, FTIR, XRD and SEM are important in characterization of nano-fertilizers (Naeem et al., 2018).

### 2.8.1 Atomic Absorption Spectroscopy

The AAS is a versatile method for measuring the concentration of several metals in sample matrix and it’s anchored upon the absorption of radiation by free metal atoms (Asare et al., 2019). It is a commonly used technique due to its sensitivity and reliability, in addition to having a low operating cost (Naeem et al., 2018). It is faster in the analysis of numerous samples and it entails the study of the absorption of characteristic radiation by neutral gaseous atoms to move from ground state to excited state. In principle, the sample solution is introduced into the flame where it is transformed into aerosol. The analyte sample is then changed into atomic vapor by the flame. The absorption of radiation by the excited neutral atoms is measured at a specific wavelength which is characteristic to metal being analyzed. For Cd and Pb analysis, their lamps of wavelengths 228.8 nm and 283.3 nm respectively can be used.

Hollow cathode lamp made of metal being analyzed is the source of radiation. At lower concentrations, the absorbance is directly proportional to the analyte concentration of metal atoms. The analysis is completed by a comparison of the absorbance of analyte samples with that of the standards samples of different known concentration using the calibration curve. According to Beer Lambert’s law at low concentration the analyte concentration is linearly correlated to the absorbance (Pramod et al., 2013), as shown in Equation 2.6.

A=-logItIo=∈Cl                                                                                         2.6

Where:-

A = Absorbance of the analyte

∈ =Molar absorptivity of the analyte (L.mol-1cm-1)

c= Concentration of the analyte (mol.L-1)

l= path length the cell (cm)

It and Io = transmitted light intensity and incident light intensity respectively

### 2.8.2 Nanoparticle Characterization Methods

For monitoring of formation and characterization of nanoparticles, several experimental techniques have been applied such as FTIR, SEM and XRD (Joshi et al., 2018; Montanzeri et al., 2010).

### 2.8.2.1 Fourier Transform Infrared Spectroscopy

Fourier transform infrared spectroscopy (FTIR) spectrum is used to characterize compounds especially organic and inorganic materials for sake of identifying functional groups. These is achieved by irradiating IR rays to interacts with sample’s, atoms, ions and functional groups which eventually vibrate their bonds to result in absorption of energy, corresponding to each vibrational mode and bending of a functional group (Tarfader et al., 2020). The principle of operation of FTIR involves the emission of IR energy from an infrared source. This IR beam is directed through a small opening to interact with the sample where particular energy frequencies are absorbed. The measurement of interferogram signal is done by the detector, then the signal is digitized to give FTIR spectrum (Joshi et al., 2018; Montanzeri et al., 2010).

From such spectra, structural information and the chemical bonds of nanoparticles obtained can be compared with those cataloged in FTIR spectra to enable the identification of the nanofertilizers, such as the bone nHA responsible for adsorption of metal ions and gradual release of nutrients (Karthik et al., 2019).

Studies done by Birendra et al. (2019) indicate that FTIR was used to characterize synthetic nHA nanoparticles by vibrational modes of OH- and PO43-. The spectra of nHA nanoparticles showed band corresponding to PO43- at 1020 cm-1, while the band at 3440 cm-1 corresponded to OH-. However there were other peaks that corresponded to symmetrical P-O stretching mode at 910-970 cm-1 and asymmetrical P-O stretching mode at 1020-1069 cm-1.

### 2.8.2.2 Scanning Electron Microscopy

The scanning electron microscopy (SEM) equipment gives the nanoparticle image which is highly magnified that looks like a real visual image by naked eyes (Yong et al., 2019). The SEM image is obtained by scanning sample surface with a raster of electron beams which interacts with the analyte atoms to produce signals with its characteristic information on composition and surface morphology (Konate et al., 2014).

Garcia et al. (2015) identified that the nanoparticle surface porosity and morphology as a primary factor for nanoparticle interfaces and their effects on their adsorption capacity. Similarly, many studies have used SEM to obtain the surface morphology and structure of the nanoparticles (Yong et al., 2019). However, poor images are obtained for nanofertilizers encapsulated or coated with conducting material, like platinum and carbon, due to their slow electron conductivity on these materials (Yong et al., 2019; Beyer et al., 2012). Beyer et al. (2012) noted that structure of nHA nanoparticles can be examined using SEM. They used it to confirm synthetic nHA particles to have size of 34.3 nm while the morphology on nHA particles was observed to be sphere-like.

### 2.8.2.3 X-Ray Diffraction

To establish the crystallite size and chemical structure for nanofertilizers X-ray diffraction (XRD) peaks were employed (Ansari et al.,2011). The obtained peaks were compared with those of the standard Joint Committee on Powder Diffraction (JCPDS) data of the diffraction pattern of hydroxyapatites (Beyer et al., 2012). Nanofertilizer samples were prepared by pulverization before being packed onto the cavity-type sample holder as indicated in Section 3.5.

The XRD operation principle is based on monochromatic X-rays interaction with that of a sample. Bombardment of the sample by the X-rays (incident) generates a detectable diffracted X-ray. The sample diffracts the X-rays in a scattering angle (Lateef et al., 2016). This angle is usually specific to the sample’s crystallite atomic structure. This X-ray is processed and finally converted to count rates so long as Braggs’s Law is converted to Scherrer equation (Equation 2.7) used in calculation of crystallite size (D)

Equation 2.7

D=KλβCos2ϴ

Where: D= is the crystallite size (nm)

K = is the Scherrer constant, 0.94 for spherical crystallographic symmetry

Λ = X-ray wavelength Cu Kꭤ =1.5406 Å

β = is line broadening at FWH

ϴ= is Bragg’s angle in degree, half of 2ϴ

# CHAPTER THREE

# METHODOLOGY

## 3.1 Research Design

A randomized complete block design was used in this study, where kales, spinach and beans were grown in two separate experimental set-ups. In one set-up, synthetic nHA was encapsulated with two commercial fertilizers NPK, DAP on one hand and in another, bone nHA with the NPK, DAP commercial fertilizers. The experiments were performed in pots under a greenhouse environment at Nyakoe, Kisii County. Growth performance parameters of the plants were measured between 30-90 days. Characterization of synthetic and bone nano-fertilizers was done using XRD, SEM and FTIR.

## 3.2 Reagents and Chemicals

Double de-ionized distilled water was obtained by a Milli-Q water distiller installed at Kenyatta University, which was used in preparation of all aqueous solutions. All used chemicals and reagents were of analytical grade. Phosphoric acid (H3PO4), calcium hydroxide (Ca(OH)2), cadmium nitrate (Cd(NO3)2), lead (II) nitrate (Pb(NO3)2), nitric (V) acid (HNO3), standards of Cd(NO3)2 and Pb(NO3)2 were used as obtained from Sigma-Aldrich Company limited, Germany. The Di-ammonium phosphate (DAP), NPK commercial fertilizers were used as supplied by YARA Fertilizer Company limited, Kenya.

## 3.3 Method Validation

#### The accuracy of AAS was investigated by spiking samples with a 1, 5, 10, 20, 50 ppm of Cd and Pb standards. Triplicate measurement of Cd and Pb levels was performed in each case. To validate the method used recovery tests, metal detection limits (3d), regression equation and correlation determination (R2) of Cd and Pb in plants leaves samples were measured and results presented in Table 4.1.

### 3.3.1 Recovery Tests

The efficiency and reliability of the AAS method was checked by the recovery tests. The 0.5 g of bean leaf powder was spiked with 1, 5, 10, 20, 50 ppm of the cadmium standard solution in triplicates. Similar procedure was repeated with bean leaves using lead standard solutions and then with kale leaves for recovery tests.

### 3.3.2 Limit of Detection of AAS

The AAS limit of detection (LOD) was determined as described by Sezgin et al. (2019). The AAS measurements for three blank samples were done in replicate and then their standard deviations were calculated. The pooled standard deviations of the blank samples were multiplied by three to obtain the limit of detection.

## 3.4 Synthesis of Hydroxyapatite Nano-fertilizers

### 3.4.1 Synthesis of Synthetic nHA Nano-fertilizers

The synthetic nHA nanoparticles were prepared by chemical precipitation as described by Ansari et al. (2011). A 100 cm3 solution of 0.67 M phosphoric acid was added dropwise at a rate of one drop per 10 seconds to a suspension of 100 cm3 of 2 M calcium hydroxide in 250 cm3 conical flask while mechanically agitating at 1000 rpm for 24 hours. The resultant synthetic nHA nanoparticles were washed three times with triple distilled water to remove any impurities. These synthetic nHA nanoparticles were put in an oven set at a temperature of 110 0C for 2 hours, before being kept at 0 oC in a freezer awaiting characterization using SEM, XRD and FTIR.

The synthetic nHA nanoparticles were mixed with a saturated solution of commercial DAP set for ultrasonic mixing of 30 kHz for 1 hour. The nHA nanoparticles were washed with triple distilled water to eliminate DAP fertilizer that was loosely held. Then the resultant nanoparticles were put in oven set at 50 0C temperature for 6 hours to dry synthetic DAP nano-fertilizers.

The procedure of encapsulation of nHA nanoparticles was repeated with dilute commercial fertilizer solutions of NPK, DAP-NPK to form synthetic NPK nano-fertilizer and synthetic NPK-DAP nano-fertilizer.

### 3.4.2 Synthesis of Bone nHA Nano-fertilizers

Bone nHA nanoparticles were prepared by using 30 kg cow bones which were cleaned, washed, dried and then ground into small pieces. Then bones were incinerated in the muffle furnace at temperature of 600 0C for 24 hours. The resultant bone ash was further ground into very fine powder using mortar and pestle. This bone powder was then mixed with distilled water at 50 % (w/w) to form a suspension of bone ash. This suspension was then milled further by vibrator for 24 hours before filtering it to get bone cakes. The filtered bone cakes were put in oven set at 80 0C temperature for 3 hours, before they were ground to nano sized bone nHA nanoparticles using mortar and pestle. The 10 kg obtained bone nHA nanoparticles were encapsulated with commercial DAP, NPK to make bone DAP nano-fertilizer, bone NPK nano-fertilizer and bone NPK-DAP nano-fertilizer as described in Section 3.4.1.

## 3.5 Nanoparticle Characterization

Nano-fertilizers were characterized according to description given by Beyer et al. (2012). The major functional groups present in the bone and synthetic nHA nano-fertilizers and their combinations were characterized by obtained spectra of FTIR (SHIMADZU FTIR 8400S Kyoto, Japan) spectrophotometer. Sample preparation of bone nHA was achieved by measuring determined amount of the nanofertilizers and homogeneously mixed with potassium bromide in a ratio of 1:50 for 5 minutes. Sample pellets were made using hand press and there after placed onto the sample holder for subsequent FTIR analysis. The spectra were obtained within the range of 250-4500 cm-1 for both bone and synthetic nHA nano-fertilizers and their combinations. FTIR functional group intensities were used to identify the encapsulated functional groups.

Scanning Electron Microscope (Zeiss Gemini SEM 500 at Indian Institute of science and Technology) was used to determine the surface morphology and particulate size of the nano-fertilizers as elaborated by Beyer et al. (2012). Powdered nano-fertilizer samples were compressed on double sided carbon tape mounted on aluminum stubs; in SEM equipment and measurements done at an accelerating voltage of 10-20 kV. The XRD equipment was also used to determine the crystallite size using a RIGAKU X-ray diffractometer (Indian Institute of science and Technology). For solid samples they are ground to fine powder using mortar and pestle. Powdered sample was compressed and packed onto the cavity-type sample holder. The compressed sample was carefully placed in appropriate sample compartment in XRD equipment to obtain XRD peaks. The obtained peaks were compared with those of the standard Joint Committee on Powder Diffraction (JCPDS) data of the diffraction pattern of hydroxyapatites.

## 3.6 Determination of Cd and Pb Uptake in Kale, Spinach and Beans

Pot greenhouse experiment was set at Nyakoe study area in Kisii County, where the sandy loamy experimental soil was obtained and oven dried to 40 oC for 48 hours until constant mass was achieved. The soil was then ground, sieved and then artificially contaminated with Cd/Pb by sprinkling with Cd/Pb contaminated water made by adding (Cd(NO3)2) and (Pb(NO3)2) salts. Contaminants in the fertilizer were not considered. The fertilizers DAP and NPK were used as supplied by YARA Fertilizer Company limited. Pot experiments were conducted with eleven treatments which were; bone nHA, bone DAP, bone NPK, bone DAP-NPK, syn nHA, syn DAP, syn NPK, syn DAP-NPK, DAP, NPK, DAP-NPK and control (without any treatment). To each treatment 20 g of nanofertilizer was added. Then the soil was mixed homogenously to have uniform nanofertilizer distribution. The study crops that were used include beans (P. Vulgaris L.), spinach (Spinacia oleracea) and kales (Brassica oleracea acephala) planted in the greenhouse study set at Nyakoe, Kisii County at temperature of averagely 27 0C. Three triplicates treatment with one seedling grown per treatment and per study crop were done. Nano-fertilizers were applied at a rate of 2.5 % (w/w) with weight of experimental soil during planting. Kales, spinach and beans were allowed to grow upto 90 days of which harvesting and plant height measurement was done three times at 30th , 60th , and 90th  day, while stem diameter, leaf diameter, number of leaves, number of pods and dry weight biomass was measured at 90th day.

### 3.6.1 Harvesting of Plant Samples

Harvesting of mature leaves were sampled in triplicates from beans (P. Vulgaris L.), spinach (Spinacia oleracea) and kales (Brassica oleracea acephala) study crops with sample size of n = 9. The harvested leaves were double washed with triple distilled water, dried at oven set at 60 0C for 3 hours. The sample was ground into fine powder then acid digested before being measured by AAS for levels of Cd and Pb.

### 3.6.2 Preparation of Standards

All the chemicals that were used to prepare standards were of analytical grade (˃98.7 %) and their solution were made using triple-distilled deionized water. The 1000 ppm cadmium standard solution was made by dissolving exactly 1.0 g of Cd(NO3)2 in aqua regia solution which is HCl and HNO3 mixed at a ratio of 1:3, and then resultant solution made up to 1 litre. Whereas 1000 ppm lead standard solution was made by dissolving exactly 1.59 g of Pb(NO3)2 in one liter of dilute solution of 1 % HNO3. Serial dilution was done on the resultant solution to get various working standards of 1, 5, 10, 15, 20, 25, 50 and 100 ppm. The absorbencies of these standards together with their concentration were used to plot the calibration curve used in determination of analytes concentration (Iqbal et al., 2019).

### 3.6.3 Sample Digestion and Heavy Metal Determination

Triplicate leave samples were digested by the procedures described by Pramod et al. (2013). Accurately weighed 2.0 g leave samples was acid digested by reacting with concentrated nitric acid until no more brown fumes were evolved. The digestion was done at temperatures of over 100 0C. The digested samples were cooled and then rinsed with 20 ml solution of 6 % nitric (v) acid. The resultant mixture was filtered and then topped into the mark of 50 ml volumetric flask with triple distilled deionized water. The digested samples were corked in plastic bottles before being stored in a freezer at KU laboratory awaiting AAS measurements. The digested samples were aspirated into the AAS and absorbance measured at wavelength of 228.80 nm for Cd and 283.30 nm for Pb.

Triplicate blanks were prepared in a similar way the samples were prepared, then the matrix introduced into the AAS equipment for the blank sample analysis, then used for method validation. The standards were the basis of calibration curves used in the determination of the concentration of Cd and Pb. The curves were obtained by plotting the absorbance against varied concentrations obtained by serial dilution of standard solutions. Calibration curves were used in determination of Cd and Pb levels. Analysis of the digested samples was done in triplicates (Asare et al., 2019; Musico et al., 2013).

## 3.7 Determination of Growth Performance

Study crops kale, spinach and beans were left to grow to 90 days at maturity stage. The growth performance parameters namely plant height, dry weight, leaf diameter and number of leaves for beans (P. Vulgaris L.), spinach (Spinacia oleracea) and kales (Brassica oleracea acephala) grown using synthetic and bone hydroxyapatite nano-fertilizers at 30, 60 and 90 day.

### 3.7.1 Plant Height

Using a tape measure, the height (cm) of the main stem of the kale (Brassica oleracea acephala) plant was measured from the soil level to the highest tip of visible leave at 30th, 60th, and 90th day according to Mohammad et al., (2019). The measurement was done in triplicates. The same procedure was applied to measure the height of beans (P. Vulgaris L.) and spinach (Spinacia oleracea).

### 3.7.2 Leaf Diameter

Leaf diameter (cm) was measured by randomly selecting kale (Brassica oleracea acephala) leaf and measured in triplicate from one leaf end to other, at every time of harvest using 30 cm ruler and recorded in respective tables. The experimental procedures were repeated with beans (P. Vulgaris L.) and spinach (Spinacia oleracea) leaf.

### 3.7.3 Number of Leaves

For kales (Brassica oleracea acephala) the physical visible leaves were counted manually in triplicates and the number of leaves per plant recorded in respective tables. For the spinach (Spinacia oleracea), all identified leaves were counted including senesced leaves. The experimental procedures were repeated with beans (P. Vulgaris L.).

### 3.7.4 Number of Pods

For beans (P. Vulgaris L.) the physical visible pods were counted manually in triplicates and the number of pods per plant recorded in respective tables.

### 3.7.5 Dry Biomass Weight

At 90th day, the kales (Brassica oleracea acephala) plants were uprooted, washed and oven-dried at 100 0C for 48 hours, and then the dry biomass was weighed in triplicates by beam balance to establish the dry weight (g). The dry weight results were recorded in respective tables. The experimental procedures were repeated with beans (P. Vulgaris L.) and spinach (Spinacia oleracea).

## 3.8 Determination of Adsorption Capacity of Nanofertilizers

The effects of various factors that affect adsorption was established such as  pH, contact time, initial heavy metal ion concentration and adsorbent dosage onto nano-fertilizers, were determined as described by Hameed et al. (2017).

### 3.8.1 Effect of pH on Removal of Metal

Effect of pH on removal of metal ions Cd2+and Pb2+was investigated at pH between 2 to 10 (Shah et al., 2011). The pH was adjusted using 0.15 M nitric (V) acid and 0.15 M sodium hydroxide solutions. A sample of 0.20 g of bone nHA and synthetic nHA was mixed with 50 mL of aqueous Cd2+ and Pb2+metal ion solutions containing 50 µg/g of test solution and buffered with 0.1 M sodium acetate (Banerjee et al., 2019). The nano-fertilizers were stirred at a 1000 rpm for 2 hour, centrifuged, filtered and concentrations of Cd2+and Pb2+measured using AAS (Das et al., 2012). Analysis was done in triplicates.

### 3.8.2 Effect of Initial Metal Concentration on Removal of Metal

Effect of Cd2+ and Pb2+ initial metal concentration was established by spiking 0.20 g of bone nHA and synthetic nHA to 50 ml of the Cd2+and Pb2+ respective metal ion solutions of between (5 - 100) µg/g buffered at optimum pH of each metal (Banerjee et al., 2019). The resultant mixture was stirred at 1000 rpm for 2 h, filtered and then concentrations levels of Cd2+and Pb2+were determined using AAS. All experiments were done in triplicates (Singh et al., 2018).

### 3.8.3 Effect of Contact Time on Removal of Metal

The rate of metal Cd2+and Pb2+adsorption was studied by spiking 0.20 g of bone nHA and synthetic nHA to 50 ml of Cd2+and Pb2+ respective metal ion solution of 50 µg/g buffered at optimum pH of each metal ion using sodium acetate (Hameed et al., 2013). The mixtures were equilibrated for predetermined time of 5 - 240 minutes in bottles on a shaker at 1000 rpm done in triplicates (Wu et al., 2012). The solutions were then centrifuged and the filtrates subjected to AAS to determine Cd2+ and Pb2+ heavy metal concentration.

### 3.8.4 Effect of Adsorbent Dosage on Removal of Metal

The effect of dosage of bone nHA and synthetic nHA adsorbents on Cd2+and Pb2+adsorption was established by varying the quantity of each nanofertilizer (0.05-1.0 g) in the test solution of 50 µg/g buffered at optimum pH of each metal using sodium acetate and then keeping the initial concentration, pH, and contact time constant (Bertazzo et al., 2010). The Cd2+and Pb2+ ions solutions were adjusted to pH 6 for Cd2+ and pH 5 for Pb2+ analysis respectively. The triplicate experiments were conducted and stirred by water bath shaker for 2 hours in plastic bottles at 1000 rpm (Benerjee et al., 2012). At the end of optimal 2 hour contact time, the nano-fertilizers were centrifuged, decanted and filtered. The concentrations of Cd2+and Pb2+ ions were measured using AAS.

## 3.9 Adsorption and Kinetic Studies

Applications of the rate equations (Equations 2.4 and 2.5) for describing the kinetics mechanism were studied at optimized conditions for Cd2+ and Pb2+ of initial concentration between 5 to 60 µg/g in triplicates (Wang et al., 2016). For these studies, 50 ml test solution at 25±0.5 °C, pH 6 in synthetic and bone nano-fertilizer adsorbents were put in a mechanical shaker and agitated between 10 minutes to 3 hours (Zhangwei et al., 2019; Benerjee et al., 2012). After 2 hours, 20 ml of the solution were removed, filtrated and measured for Cd2 and Pb2+ of equilibrium concentration. The amount adsorbed at equilibrium within 2 hours optimal time was calculated by Equation 2.2 (Langmuir) and Equation 2.3 (Freundlich isotherm).

## 3.10 Nutrients Release Levels by Nano-fertilizers

The nutrient release rates were performed for bone nHA and synthetic nHA nanofertilizer and their combinations as described by Nilwala et al. (2011) to determine the releasing pattern of nutrients. Triplicate samples of soil each weighing 400 g was obtained from the Cd/Pb contaminated experimental soil. The samples were mixed thoroughly with 40 g of bone nHA nanofertilizer for homogeneity. The samples were placed into separate 500 ml separatory funnel columns that were saturated with distilled water to reach 85 % soil-water saturation point. The columns were allowed to elute as described by Nilwala et al., (2011) using a controlled tap at a rate of 5 drops per minute for 24 hours on every 5th day. The collection of elute repeated for a period of 5 days at the intervals of 5, 10, 15, 20, 25, 30, 35 and 40 days, respectively. Then 100 ml distilled water was added after every 5 days to keep experimental soil saturated with water.

The concentration levels of NO3-, PO43- in the eluant was measured using a UV-visible spectrophotometer while that of K+ release rate of the eluant was measured using FAAS. The above procedure experiment on nutrient release was repeated in triplicates with the addition of 40 g various treatments to Cd/Pb experimental soil, NPK bone nHA, DAP bone nHA, DAP-NPK bone nHA, NPK Syn nHA, DAP Syn nHA, DAP-NPK Syn nHA, NPK, DAP, a mixture of DAP-NPK commercial fertilizer, to 400 g of sample soil (Tarafder et al., 2020; Nilwala et al., 2011).

## 3.11 Data Analysis

The obtained data was analyzed by SPSS version 22 which employed ANOVA (one-way) to compare the means and percentages of Cd and Pb uptake reductions, growth parameters (plant height, plant leave diameter, plant number of leaves and bean number of pods) with mean separations by standard deviation (Ewa et al., 2019; Saghi et al., 2016). When the values of P<0.05, it implies the means are significantly different, (ANOVA, p=0.05). The concentrations of Cd and Pb were reported in µgg-1.

# CHAPTER FOUR

# RESULTS AND DISCUSSIONS

## 4.1 Introduction

The results addressing the objectives (i-v) stated in Section 1.4.2 are presented in figures and tables as discussed in this chapter.

## 4.2 Method Validation

Table 4.1 shows regression equations of calibration curves of lead and cadmium which were used to calculate Cd and Pb concentration levels obtained from crop leaves. Similarly, recovery tests, metal detection limits (3d), correlation determination (R2) and metal percentage recoveries for leaves and soil samples.

#### Table 4.1: Method Validation parameters

|  | Metal | Regression equation | Detection limit (3d) µgg-1 | Correlation determination (R2) | % Recovery |
| --- | --- | --- | --- | --- | --- |
| Kale leaves | Cd | y = 0.79x +0.13 | 0.62±0.0020 | 0.997 | 97.0-100 |
|  | Pb | y = 0.81x + 0.18 | 0.35±0.0011 | 0.998 | 97.1-100 |
| Bean leaves | Cd | y = 0.79x +0.35 | 0.72±0.0015 | 0.997 | 98.1-100 |
|  | Pb | y = 0.81x + 0.89 | 0.39±0.0022 | 0.998 | 99-100 |

The LODs ranged from 0.35 to 0.72 and this  was higher than to those reported by Sezgin et al.(2019) who obtained 0.036±0.0011 and 0.025±0.0015 µgg-1 for Cd and Pb respectively. The coefficient of correlation (R2) values were above 0.996 (R2˃0.996), indicating at least 99.6 % linearity of absorbance against concentration (Sezgin et al., 2019). The percentage recoveries were between 97.0 and 100 % implying that the methods employed in this study had permissible precision and accuracy (Qi et al., 2020).

## 4.3 Nanoparticle Characterization

### 4.3.1 SEM Analysis

Figure 4.1 to 4.3 shows SEM (Scanning Elecron Microscopy) images of nanoparticles using Zeiss Gemini SEM 500 (Indian Institute of science and Technology).

b

a

Figure 4.1: (a) SEM image of bone nHA and (b) SEM image of synthetic nHA

b

a

Figure 4.2: (a) SEM image of bone DAP Nano and (b) SEM image of synthetic DAP Nano

b

a

##### Figure 4.1: (a) SEM image of bone NPK Nano and (b) SEM image of synthetic NPK Nano

The SEM (Scanning Elecron Microscopy) images show the nanoparticles consist of constricted spherical crystallites with an average size of 24-35 nm and they show formation of agglomerates. The synthetic nano-fertilizers surface texture and morphology have rigid, rough and constricted agglomerated surface (Fig 4.1(b) and 4.3(b)). However, the bone nano-fertilizers have a slight change in surface morphology with stronger, rougher and more rigid pocket like adsorption sites. This can be attributed to natural strength and structure of nanohydroxyapatite bones. The bone nanofertilizers and their combination had lower level of agglomeration than synthetic nHA nanofertilizers and their combinations. This signifies that the bone nHA nanofertilizers have higher number of adsorption sites than synthetic nHA nanofertilizers (Tarfadar et al., 2020).

### 4.3.2 XRD Analysis

Figure 4.4 to 4.7 shows X-ray diffraction (XRD) micrograph observed using an X-ray diffractometer (RIGAKU) at Indian Institute of science and Technology.

b

a

Bragg’s angle

Bragg’s angle

##### Figure 4.2: (a): XRD image of bone nHA and (b) XRD image of synthetic nHA

b

a

Bragg’s angle

Bragg’s angle

##### Figure 4.3: (a): XRD image of bone DAP Nano and (b) XRD image of synthetic DAP Nano

b

a

Bragg’s angle

Bragg’s angle

##### Figure 4.4: (a) XRD image of bone NPK nano and (b) XRD image of synthetic NPK Nano

b

a

Bragg’s angle

Bragg’s angle

##### Figure 4.5: (a) XRD image of bone NPK-DAP Nano and (b) XRD image of synthetic NPK-DAP Nano

The XRD patterns of bone and synthetic nano-fertilizers indicate the presence of amorphous nHA. The sharp peaks from 24.24 – 35.35 nm revealed that the nano crystallite were formed (Table 4.2). The reflection planes corresponding to the characteristic XRD spectral peaks of bone and synthetic nano-fertilizer are shown in Fig.4.4 - 4.7. The standard JCPDS file no. (09-0432) is used to identify the observed diffraction peaks, which are eventually assigned to crystallite nHA nanoparticles. The sharp XRD characteristic peaks that appeared at 260, 32.50 and 390 on the bone and synthetic nano-fertilizer corresponding to the peaks of nano-hydroxyapatite powder (Tarafder et al., 2020). The XRD patterns show peaks with higher intensities which conforms to the nHA nano sized particles of highly crystallite nature. Table 4.2 shows crystallite size of studied nanofertilizers using a sample size n = 3.

#### Table 4.2: Nano-fertilizer particle sizes determined from XRD analysis

| NANOPARTICLE | AVERAGE PARTICLE DIAMETER Mean ± SD(nm), n=3 |
| --- | --- |
| Bone nHA | 24.25±0.14a |
| Syn nHA | 27.35±0.24c |
| Bone nHA +DAP | 25.11±0.19b |
| Syn nHA +DAP | 29.24±0.42c |
| Bone nHA+ NPK | 28.57±0.31c |
| Syn nHA+ NPK | 31.50±0.34d |
| Bone nHA+DAP+NPK | 29.57±0.09c |
| Syn nHA+DAP+NPK | 34.14±0.11d |
|  | P-value˂0.01 |

Means ± SD superscripted with similar small letters within the same column are not significantly different at p =0.05 (Anova).

The crystallite size ranged between 24 to 34 nm as calculated by Scherrer equation from peaks obtained in the XRD peaks. The bone nanoparticles were significantly smaller in crystallite size in comparison with their respective synthetic nanoparticles. This signifies that the bone nanoparticles have higher number of adsorption sites and the contact surface area to volume ratio, making it more effective in heavy metal adsorption and gradual release of nutrients. The related results were posted by Tarfadar et al., 2020 that got non-significantly difference in synthetic nHA nanoparticle crystallite size ranging from 20 – 40 nm.

### 4.3.3 FTIR Analysis

Figure 4.8(a)-4.8(h) shows the spectra that were obtained of bone and synthetic nanoparticles and their combinations using SHIMADZU FTIR 8400S (Kyoto, Japan) spectrophotometer, ran within the range of 250 cm-1 to 4500 cm-1.

d

c

b

a

f

e

g

h

##### Figure 4.6: FTIR images of various nanofertilizers in the order (a) bone nHA, (b)synthetic nHA, (c)bone DAP nano, (d) synthetic DAP nano, (e) bone NPK nano, (f) synthetic NPK nano,(g) bone NPK-DAP nano, (h) synthetic NPK-DAP nano respectively.

From micrographs, the functional groups were assigned using the peaks obtained from bone nHA nanofertilizers. A strong peak at 3455.53 cm-1 was signifying presence of the stretching alcohol group (O-H) found in apatite while the peak at 2066.80 cm-1 was assigned to stretching alkyne (-C≡C-) group. The strong peak at 1640.49 cm-1 was assigned to Carbonyl group (-C=O-) while the medium peak at 1407.10 cm-1 signified presence of amide. The peak at 1289.34 cm-1 showed presence of C-N stretching aromatic amines. The peaks at 1093.66 and 1047.10 cm-1 indicated presence of C-N which is stretching aliphatic amine and PO43- respectively. The C-H bend alkenes group was noted at 874.73 cm-1 for synthetic NPK-DAP nanofertilizer. The peak at 468.71 cm-1 signified C-F stretch of alkynes group attributed to peak interaction between bone NPK-DAP nanofertilizer and fluoride in hydroxyapatites. Similar trends were observed in all other FTIR nanohydroxyapatite nanoparticles since the encapsulation with DAP and NPK fertilizers can’t change the structure of hydroxyapatites, but increased their intensities. Birendra et al. (2019) obtained related results in characterization of synthetic hydroxyapatites that had major functional groups as OH and PO43-.

## 4.4 Cadmium and Lead Uptake

### 4.4.1 Uptake Levels of Cd in Crops Grown Using Nano-fertilizers

Tables 4.3 to 4.5 shows the uptake levels of cadmium (Cd) in kale, spinach and bean leaves grown using various treatments of the synthetic (Syn nHA) and bone hydroxyapatite (Bone nHA) nano-fertilizer at 30, 60 and 90 day. Table 4.6 shows a comparison of Cd uptake levels of kale, spinach and beans at 90th day

#### Table 4.3: Levels of cadmium in kale leaves grown using nano-fertilizers at 30, 60 and 90 day

| TREATMENT | [Cd] Mean ± SD(µgg-1) n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | 30 days | 60 days | 90 days |  |
| Bone nHA | 40.12±2.03aC | 16.33±0.31aB | 2.94±0.29aA | P-value ˂0.01 |
| Syn nHA | 51.18±1.52cC | 20.17±2.30bB | 3.91±1.92bA |  |
| Bone nHA +DAP | 45.66±1.07bC | 19.97±0.93bB | 3.29±0.72bA |  |
| Syn nHA +DAP | 49.08±0.75bC | 23.83±2.19cB | 5.16±1.64cA |  |
| Bone nHA+ NPK | 46.00±1.03bC | 20.74±1.58bB | 6.18±1.13dA |  |
| Syn nHA+ NPK | 51.21±1.14dC | 24.81±0.38cB | 7.42±0.30eA |  |
| Bone nHA+DAP+NPK | 42.90±0.34aC | 20.03±2.14bB | 4.61±1.62cA |  |
| Syn nHA+DAP+NPK | 50.76±2.61dC | 23.45±5.49cB | 4.57±3.58cA |  |
| DAP | 65.23±3.31gC | 43.25±2.32eB | 38.66±1.79gA |  |
| NPK | 61.75±2.76fC | 44.26±2.02eB | 37.38±1.58gA |  |
| DAP+NPK | 59.46±0.39fC | 68.40±3.73fB | 37.62±2.87gA |  |
| Non-treated control | 52.20±2.92eC | 38.74±1.18dB | 30.15±0.87fA |  |
|  |  | P-value˂0.01 |  |  |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

#### Table 4.4: Levels of cadmium in spinach leaves grown using nano-fertilizers at 30, 60 and 90 day

| TREATMENT | [Cd] Mean ± SD(µgg-1) n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | 30 days | 60 days | 90 days |  |
| Bone nHA | 57.12±2.01aC | 18.51±1.13aB | 3.56±0.93aA | P-value ˂0.01 |
| Syn nHA | 60.18±1.48bC | 24.03±1.28cB | 5.88±0.91cA |  |
| Bone nHA +DAP | 58.66±1.05aC | 20.45±0.49bB | 4.35±0.38bA |  |
| Syn nHA +DAP | 62.08±0.86bC | 24.77±0.97cB | 6.35±0.79dA |  |
| Bone nHA+ NPK | 57.00±1.02aC | 19.61±0.47aB | 3.69±0.40aA |  |
| Syn nHA+ NPK | 63.21±1.23bC | 21.44±0.57bB | 7.93±0.42eA |  |
| Bone nHA+DAP+NPK | 57.90±0.31aC | 19.26±0.16aB | 3.94±0.23aA |  |
| Syn nHA+DAP+NPK | 62.76±2.55bC | 24.00±0.89cB | 7.70±0.63dA |  |
| DAP | 80.23±3.34eC | 60.18±2.65fB | 49.15±2.12gA |  |
| NPK | 76.75±2.79dC | 56.50±2.17eB | 49.88±1.58gA |  |
| DAP+NPK | 74.46±0.43dC | 55.13±0.31eB | 48.75±0.24gA |  |
| Non-treated control | 67.20±2.87cC | 48.22±2.26dB | 37.93±1.64fA |  |
|  |  | P-value˂0.01 |  |  |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

#### Table 4.5: Levels of cadmium in bean leaves grown using nano-fertilizers at 30, 60 and 90 day

| TREATMENT | [Cd] Mean ± SD(µgg-1) n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | 30 days | 60 days | 90 days |  |
| Bone nHA | 33.70±4.50aC | 6.47±3.00aB | 2.20±2.22aA | P-value ˂0.01 |
| Syn nHA | 36.44±2.55bC | 9.90±1.59bB | 2.91±1.16bA |  |
| Bone nHA +DAP | 35.52±2.48aC | 9.95±1.71bB | 3.85±1.28cA |  |
| Syn nHA +DAP | 38.65±0.88bC | 12.10±0.59cB | 5.32±0.41dA |  |
| Bone nHA+ NPK | 34.57±1.92aC | 10.23±1.35bB | 4.22±1.02cA |  |
| Syn nHA+ NPK | 38.97±0.82bC | 9.09±0.55bB | 6.92±0.40eA |  |
| Bone nHA+DAP+NPK | 33.05±4.83aC | 7.48±3.33aB | 4.21±2.47cA |  |
| Syn nHA+DAP+NPK | 37.94±1.71bC | 10.37±1.12bB | 5.81±1.16dA |  |
| DAP | 50.84±3.02dC | 39.03±2.52fB | 32.38±1.89hA |  |
| NPK | 51.69±4.35dC | 33.64±3.79fe | 28.64±2.87gA |  |
| DAP+NPK | 50.74±1.23dC | 34.41±0.95fe | 29.54±0.72gA |  |
| Non-treated control | 45.75±2.95cC | 28.27±2.27dB | 22.82±1.74fA |  |
| P-value˂0.01 |  |  |  |  |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

#### Table 4.6: Comparison of cadmium uptake in bean, kale and spinach leaves grown using nano-fertilizers at 90th day

| TREATMENT | [Cd] Mean ± SD(µgg-1) n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | Bean | Kale | Spinach |  |
| Bone nHA | 2.20±2.22aA | 2.94±0.29aA | 3.56±0.93ab | P-value ˂0.01 |
| Syn nHA | 2.91±1.16bA | 3.91±1.92bB | 5.88±0.91cC |  |
| Bone nHA +DAP | 3.85±1.28cA | 3.29±0.72bA | 4.35±0.38bB |  |
| Syn nHA +DAP | 5.32±0.41dA | 5.16±1.64cA | 6.35±0.79dB |  |
| Bone nHA+ NPK | 4.22±1.02cA | 6.18±1.13dB | 3.69±0.40Aa |  |
| Syn nHA+ NPK | 6.92±0.40eA | 7.42±0.30eA | 7.93±0.42eA |  |
| Bone nHA+DAP+NPK | 4.21±2.47cA | 4.61±1.62cA | 3.94±0.23aA |  |
| Syn nHA+DAP+NPK | 5.81±1.16dA | 4.57±3.58cA | 7.70±0.63dB |  |
| DAP | 32.38±1.89hA | 38.66±1.79gB | 49.15±2.12gC |  |
| NPK | 28.64±2.87gA | 37.38±1.58gB | 49.88±1.58gC |  |
| DAP+NPK | 29.54±0.72gA | 37.62±2.87gB | 48.75±0.24gC |  |
| Non-treated control | 22.82±1.74fA | 30.15±0.87fA | 37.93±1.64fA |  |
| P-value˂0.01 |  |  |  |  |

Means ± SD superscripted with similar small letters within the same are not significantly different at p =0.05 (Anova).

Table 4.3 indicate that the mean level of Cd (µgg-1) in kale leaves grown in soils treated with Syn nHA and Bone nHA nano-fertilizers with their combination DAP and NPK ranged from 51.21±1.14 (Syn nHA+ NPK at 30 day) to 2.94±0.29 (bone nHA at 90 day). The mean levels of Cd (µgg-1) in spinach (Table 4.4) ranged from 63.21±1.23 µgg-1 (Syn nHA +NPK at 30 day) to 3.56±0.93 (bone nHA at 90 day) while in beans (Table 4.5) the range was from 38.97±0.82 (Syn NPK nano-fertilizer at 30 day) to 2.20±2.22 µgg-1 (bone nHA at 90 day). At 90th day (Table 4.6) all the plant leaves grown using nano-fertilizers had Cd uptake levels that were within FAO/WHO permissible levels of 10 µgg-1.

In principle, there was a higher significant difference in reduction of the uptake of Cd in the plants with the growth period than the control (p<0.01), signifying the effectiveness of nano-fertilizers in immobilizing Cd (Sun et al., 2020; Zahra et al., 2019). The reduction over the growth period can also be attributed to the nano-fertilizers having longer contact time for the adsorption of Cd2+ thereby reducing their mobility and eventual uptake in plants. Nano-fertilizers have numerous adsorption, chelation and complexation sites that immobilize Cd2+ thereby reducing its uptake in plants (Zahra et al., 2019). The % reduction (72.07 to 87.60 % in kale) (Appendix I) and (76.46 to 87.98 % in spinach) (Appendix I) was not only highest for the kale grown using bone nHA but it was observed that during the growth period (30-90 days) of the plant, bone nHA showed significantly lower levels (µgg-1) of Cd (40.12±2.03) at 30 days, 16.33±0.31 at 60 days and 2.94±0.29 at 90 days) for the kales in comparison to all other treatments.. Sun et al. (2020) reduced Cd, uptake by 62 % using nano Fe3O4(Gil-Díaz et al., 2017;Saghi et al., 2016). This was significantly lower % reduction than those obtained in this study, signifying effectiveness of bone nanofertilizers.

Table 4.6 shows that Cd uptake in spinach at 90th day was significantly higher than in kales for respective treatments. This is because spinach is a higher heavy metal accumulator (Sun et al., 2020; Zhang et al., 2019). However, Cd uptake in bean was lowest in comparison with kales and spinach grown in respective treatments, since beans are least heavy metal accumulators (Rizwan et al., 2017). Rizwan et al. (2017) used zinc–lysine nanoparticles to reduced Cd in green pepper by 6.9 % to 11.6 % and eggplant fruits by 15.3 % to 15.6 % respectively which was significantly lower that results obtained in this study. Other studies of using nanoparticles have recorded signiﬁcantly lower % reduction of Cd compared to this study. For instance, Wang et al.(2016) used silicon nanoparticle in rice, to decrease Cd uptake by 59.25 %. In wheat Du et al.(2019) used ZnO to reduced Cd by 28.1 %, Saifullah et al. (2016) showed Cd, uptake reduction of 74 % using ZnO nanoparticles, while Naeem et al. (2018) used nano SiO2 to reduce Cd uptake by 28 %. Zhangwei et al. (2019) reduced Cd uptake in rice by 30.7 % using synthetic nHA. Zang et al. (2019) showed Cd uptake reduction of 12.4 % in spinach using TiO2 nanoparticles.

The Bone nHA had significantly higher % Cd reduction than the Syn nHA (p<0.01). At 90 days in kales, the Cd uptake was significantly lower (2.94±0.29 µgg-1) for Bone nHA than Syn nHA (4.91±1.92 µgg-1). This is attributed to bone nHA having higher stability, higher number of adsorption sites and larger contact surface area exposed to volume ratio for adsorption, chelation and complexation of Cd2+compared to synthetic nHA, thereby reducing Cd uptake in kales (Zahra et al., 2019). There was variation in Cd uptake among the nano-fertilizer treatments due to the differences in the type of amendment that varied number of adsorption sites as per treatment. This elaborates that the number of adsorption sites varies widely depending on ameliorate added to the pots.

### 4.4.2 Uptake Levels of Pb in Plant Leaves Grown Using Nano-fertilizers

Tables 4.7, 4.8 and 4.9 shows the uptake levels of lead (Pb) in kale, spinach and bean leaves grown using various treatments of Syn nHA and Bone nHA at 30, 60 and 90 day. Table 4.10 shows a comparison of Pb uptake  of the crops at 90th day

#### Table 4.7: Levels of lead in kale leave grown using nano-fertilizers at 30, 60 and 90 day

| TREATMENT | [Pb] Mean ± SD(µgg-1) n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | 30 days | 60 days | 90 days |  |
| Bone nHA | 33.54±1.07aC | 11.69±0.59aB | 2.74±0.29aA | P-value ˂0.01 |
| Syn nHA | 38.42±1.83bC | 15.66±0.49bB | 3.99±0.72bA |  |
| Bone nHA +DAP | 38.21±0.70bC | 15.21±3.15bB | 5.18±1.13cA |  |
| Syn nHA +DAP | 40.07±1.47cC | 16.95±0.83bB | 4.61±1.62cA |  |
| Bone nHA+ NPK | 39.34±0.94bC | 16.29±0.50bB | 3.91±1.92bA |  |
| Syn nHA+ NPK | 42.44±1.13dC | 18.40±1.88cB | 5.16±1.64cA |  |
| Bone nHA+DAP+NPK | 38.64±2.11bd | 15.15±1.32bB | 3.57±3.58bA |  |
| Syn nHA+DAP+NPK | 42.38±1.73dC | 18.15±0.77cB | 5.42±0.30cA |  |
| DAP | 69.46±1.13gC | 52.88±0.94fB | 38.66±1.79eA |  |
| NPK | 69.31±2.15gC | 52.76±1.79fB | 37.38±1.58eA |  |
| DAP+NPK | 56.33±0.05fC | 41.95±4.21eB | 37.62±2.87eA |  |
| Non-treated control | 48.37±1.15eC | 36.93±0.76dB | 30.15±0.87dA |  |
|  |  | P-value˂0.01 |  |  |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

#### Table 4.8: Levels of lead in spinach leaves grown using nano-fertilizers at 30, 60 and 90 day

| TREATMENT | [Pb] Mean ± SD(µgg-1) n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | 30 days | 60 days | 90 days |  |
| Bone nHA | 39.02±1.48aC | 20.55±0.93aB | 3.53±0.97aA | P-value ˂0.01 |
| Syn nHA | 49.11±2.53bC | 23.29±0.47bB | 5.91±0.43bA |  |
| Bone nHA +DAP | 45.26±1.75bC | 20.65±1.11aB | 6.04±0.86bA |  |
| Syn nHA +DAP | 67.06±4.9dC | 28.32±0.95cB | 9.56±0.84cA |  |
| Bone nHA+ NPK | 46.42±1.45bC | 21.31±0.91aB | 5.58±0.83bA |  |
| Syn nHA+ NPK | 63.79±4.77cC | 28.66±0.96cB | 9.78±0.58cA |  |
| Bone nHA+DAP+NPK | 48.83±0.79bC | 23.10±0.51bB | 6.42±0.90bA |  |
| Syn nHA+DAP+NPK | 69.05±4.23dC | 25.62±0.83bB | 8.97±0.58cA |  |
| DAP | 69.15±1.21dC | 54.88±0.96eB | 42.73±0.75deA |  |
| NPK | 73.84±1.99eC | 60.04±1.62fB | 44.62±1.16eA |  |
| DAP+NPK | 63.38±1.29cC | 51.86±1.18dB | 39.89±0.91dA |  |
| Non-treated control | 70.43±1.95eC | 51.18±1.50dB | 39.57±1.02dA |  |
|  |  | P-value ˂0.01 |  |  |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

#### Table 4.9: Levels of lead in bean leaves grown using nano-fertilizers at 30, 60 and 90 day

| TREATMENT | [Pb] Mean ± SD(µgg-1) n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | 30 days | 60 days | 90 days |  |
| Bone nHA | 31.27±1.16aC | 5.95±0.93aB | 1.64±1.11aA | P-value ˂0.01 |
| Syn nHA | 41.00±2.8cC | 9.76±1.20cB | 2.33±0.70bA |  |
| Bone nHA +DAP | 31.63±1.45aC | 6.65±1.11aB | 1.93±0.73aA |  |
| Syn nHA +DAP | 43.40±1.73cC | 10.72±0.82eB | 2.94±0.52bA |  |
| Bone nHA+ NPK | 35.41±1.45bC | 7.31±0.91abB | 2.97±0.98bA |  |
| Syn nHA+ NPK | 46.46±2.15cdC | 9.18±1.05cB | 4.21±0.68cA |  |
| Bone nHA+DAP+NPK | 36.48±1.12bC | 6.10±0.51aB | 1.65±0.99aA |  |
| Syn nHA+DAP+NPK | 44.20±6.08dC | 9.98±2.70cB | 2.50±1.75bA |  |
| DAP | 51.90±4.10eC | 54.88±0.96eB | 32.21±2.63eA |  |
| NPK | 52.15±1.09eC | 60.04±1.62fB | 34.36±1.16eA |  |
| DAP+NPK | 51.59±2.77eC | 51.86±1.18eB | 31.92±1.57eA |  |
| Non-treated control | 50.52±1.31eC | 47.18±1.50dB | 27.25±0.99dA |  |
|  |  | P-value ˂0.01 |  |  |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

#### Table 4.10: Comparison of lead uptake in bean, kale and spinach leaves grown using nano-fertilizers at 90th day

| TREATMENT | [Pb] Mean ± SD(µgg-1) n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | Bean | Kale | Spinach |  |
| Bone nHA | 1.64±1.11aA | 2.74±0.29aA | 3.53±0.97aB | P-value ˂0.01 |
| Syn nHA | 2.33±0.70bA | 3.99±0.72bB | 5.91±0.43bC |  |
| Bone nHA +DAP | 1.93±0.73aA | 5.18±1.13cB | 6.04±0.86bB |  |
| Syn nHA +DAP | 2.94±0.52bA | 4.61±1.62cB | 9.56±0.84cC |  |
| Bone nHA+ NPK | 2.97±0.98bA | 3.91±1.92bB | 5.58±0.83bC |  |
| Syn nHA+ NPK | 4.21±0.68cA | 5.16±1.64cA | 9.78±0.58cB |  |
| Bone nHA+DAP+NPK | 1.65±0.99aA | 3.57±3.58bB | 6.42±0.90bC |  |
| Syn nHA+DAP+NPK | 2.50±1.75bA | 5.42±0.30cB | 8.97±0.58cC |  |
| DAP | 32.21±2.63eA | 38.66±1.79eB | 42.73±0.75deC |  |
| NPK | 34.36±1.16eA | 37.38±1.58eA | 44.62±1.16eB |  |
| DAP+NPK | 31.92±1.57eA | 37.62±2.87eB | 39.89±0.91dB |  |
| Non-treated control | 27.25±0.99dA | 30.15±0.87dB | 39.57±1.02dC |  |
| P-value˂0.01 |  |  |  |  |

Means ± SD superscripted with similar small letters within the same column are not significantly different at p =0.05 (Anova).

Table 4.7 indicate the mean of Pb (µgg-1) in kale leaves grown in soils treated with Syn nHA, bone nHA nano-fertilizers and their DAP/NPK combinations (Table 4.7) ranged from 42.44±1.13 (Syn nHA NPK at 30 day) to 2.74±0.57 µgg-1 (Bone nHA at 90 day), while in Spinach the mean shown on Table 4.8 of Pb (µgg-1) ranged from 69.05±4.53 (syn nHA DAP-NPK at 30 day) to 3.53±0.97 µgg-1 (bone nHA at 90 day). However, for beans (Table 4.9) the mean Pb concentration levels ranged from 46.46±2.15 (Syn nHA NPK at 30 day), to 1.64±1.11 µgg-1 (bone nHA at 90 day). The % reduction of Pb uptake in beans for pots treated with nano-fertilizer treatments ranged from 80.88 to 92.51 % (Appendix I).

The % reduction of Pb uptake for treatments with nano-fertilizers ranged from 74.22 to 86.82 % (Table on Appendix I) in kale. Sun et al. (2020) showed immobilization of Pb, increased by more than 74 % through application of biochar nanoparticles this depending on dosage and pH (Gil-Díaz et al., 2017;Saghi et al., 2016). The % reduction was not only highest for the kale plant grown using bone nHA but it was observed (Table 4.7) that during the growth period (30-90 days) of the kale plant, bone nHA showed significantly lower levels of Pb (µgg-1) (33.54±1.07 at 30 days, 11.69±0.59 at 60 days and 2.74±0.29 at 90 days) in comparison to all other treatments. These values are significantly lower than those obtained in beans in the other treatments. Bone nHA had statistically significantly lower Pb levels (p<0.01) than Syn nHA and its combinations. At 90 day all the plant leaves obtained from nano-fertilizer treated pots had Pb uptake levels that were within FAO/WHO permissible level of 10 µgg-1 at maturity. The observations on the Pb uptake in the plants were  having similar trends to those of Cd (Table 4.4 to Table 4.5) and they are supported by a similar discussion in Section 4.4.1.

Pb uptake levels were lower in comparison to Cd uptake levels in the respective treatments. This is attributed to the lower mobility of Pb2+ in comparison with Cd2+ which has higher mobility. Similarly Pb2+ does not protonate the nano-fertilizer adsorption surface to make it positively charged. Hence there is reduced repulsion between the Pb2+ with the nanofertilizer surface (Qi et al., 2020; Mohammad et al., 2019). Other researchers have used nanoparticles to lower Pb uptake in the study plants. For example, Zhangwei et al. (2019) reduced Pb uptake in soy bean by 58.1 % using synthetic nHA nanoparticles while commercial fertilizers increased Pb uptake by 14 %. Similarly, nanoparticles have been used to immobilize Pb heavy metals like in the research conducted by Qi et al.(2020) who used composite nanoparticles to immobilize heavy metals in experimental soils while Konate et al.(2014) used magnetite nanoparticles to immobilize heavy metals and enhance growth in plants.

## 4.5 Growth Performance of Crops Grown Using Nano-fertilizers

### 4.5.1 Plant Height Growth Performance

The height growth performance of kales, spinach and beans grown in a greenhouse at 27 0C using Synthetic and bone hydroxyapatite nano-fertilizers at 30, 60 and 90 days are presented for kale height (Tables 4.11), spinach height (Table 4.12), bean height (Table 4.13).

#### Table 4.11: The 30, 60, 90 day Heights (cm) for kales grown using nano-fertilizers

| TREATMENT | Height; Mean± SD (cm) n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | 30 days | 60 days | 90 days |  |
| Bone nHA | 29.67±1.20bA | 67.00±2.52eB | 88.00±2.65eC | P-value ˂0.01 |
| Syn nHA | 25.33±0.88aA | 63.33±1.45dB | 83.67±3.18dC |  |
| Bone nHA +DAP | 31.00±1.15cA | 68.33±2.03eB | 87.67±1.76fC |  |
| Syn nHA +DAP | 26.67±1.76aA | 65.67±3.18deB | 83.67±0.88dC |  |
| Bone nHA+ NPK | 31.10±1.53cA | 69.67±3.48dB | 97.33±1.45hC |  |
| Syn nHA+ NPK | 26.67±3.18aA | 56.33±1.76cB | 93.00±1.15gC |  |
| Bone nHA+DAP+NPK | 30.00±1.15cA | 64.00±3.21deB | 88.00±1.53fC |  |
| Syn nHA+DAP+NPK | 26.67±1.76aA | 57.67±2.85cB | 70.33±0.88cC |  |
| DAP | 35.00±0.58dA | 39.00±0.58bB | 46.00±1.73bC |  |
| NPK | 28.00±1.53bA | 41.00±1.15bB | 44.67±1.86bC |  |
| DAP+NPK | 28.67±2.19bA | 40.00±0.58bB | 46.67±1.45bC |  |
| Non-treated control | 25.67±0.88aA | 30.00±0.58aB | 33.00±1.15aC |  |
|  |  | P-value ˂0.01 |  |  |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

#### Table 4.12: The 30, 60, 90 day Heights (cm) for spinach grown using nano-fertilizers

| TREATMENT | [Height] Mean± SD (cm) n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | 30 days | 60 days | 90 days |  |
| Bone nHA | 14.33±0.88cA | 29.33±1.45eB | 44.67±1.76efC | P-value ˂0.01 |
| Syn nHA | 12.33±0.88bA | 26.33±1.20dB | 40.00±0.58eC |  |
| Bone nHA +DAP | 13.33±1.20bcA | 29.00±1.15eB | 43.33±1.45eC |  |
| Syn nHA +DAP | 11.67±0.88abA | 26.00±0.58dB | 40.67±1.76eC |  |
| Bone nHA+ NPK | 13.67±1.20bcA | 33.00±1.00fB | 49.33±1.20fC |  |
| Syn nHA+ NPK | 10.33±0.88aA | 28.67±0.88eB | 33.00±1.15dC |  |
| Bone nHA+DAP+NPK | 13.00±0.58bcA | 28.33±1.20eB | 45.00±1.15defC |  |
| Syn nHA+DAP+NPK | 11.67±0.88bA | 21.67±1.45cB | 30.00±0.58cC |  |
| NPK | 13.00±0.58bcA | 21.33±0.88cB | 29.33±0.88cC |  |
| DAP+NPK | 12.00±0.58bA | 21.33±1.20cB | 28.33±1.20cC |  |
| Non-treated control | 10.67±0.88aA | 16.67±0.88AaB | 20.00±0.58aC |  |
|  |  | P-value ˂0.01 |  |  |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

#### Table 4.13: The 30, 60, 90 day Heights (cm) for bean grown using nano-fertilizers

| TREATMENT | [Height] Mean± SD (cm) n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | 30 days | 60 days | 90 days |  |
| Bone nHA | 51.67±1.45dA | 83.33±1.20fB | 100.67±2.03fC | P-value ˂0.01 |
| Syn nHA | 41.67±1.20bA | 76.33±0,88eB | 92.33±0.88eC |  |
| Bone nHA +DAP | 52.00±1.53dA | 84.33±1.20fB | 104.33±0.88gC |  |
| Syn nHA +DAP | 42.33±1.20bA | 76.67±2.19eB | 93.67±2.73eC |  |
| Bone nHA+ NPK | 43.67±1.45cA | 75.00±1.53deB | 105.67±1.45gC |  |
| Syn nHA+ NPK | 42.67±1.76bA | 72.67±1.45dB | 93.33±1.86dC |  |
| Bone nHA+DAP+NPK | 44.00±1.53cA | 79.67±0.88eB | 96.00±1.15efC |  |
| Syn nHA+DAP+NPK | 42.00±0.58bcA | 71.00±2.65dB | 88.00±2.08dC |  |
| NPK | 40.67±0.88bcA | 44.00±1.15cB | 45.33±1.20cC |  |
| DAP+NPK | 37.00±2.08bA | 44.33±0.67cB | 46.00±0.58cC |  |
| Non-treated control | 20.33±0.88aA | 26.00±1.53aB | 28.33±1.45aC |  |
|  |  | P-value ˂0.01 |  |  |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

The Table 4.11 indicates the mean heights in kales grown in soils treated with Syn nHA, bone nHA nano-fertilizers and their DAP/NPK combinations ranged from 25.33±0.88 cm (synthetic nHA at 30 day) to 97.33±1.45 cm (Bone nHA NPK nano-fertilizer at 90 day). For spinach (Table 4.12) it ranged from 10.33±0.88 cm (Syn nHA+NPK nano-fertilizer at 30 day) to 49.33±1.20 cm (Bone nHA+NPK nano-fertilizer at 90 day). For the beans (Table 4.13) the range was 41.67±1.20 cm (syn nHA at 30 day).to 105.67±1.45 cm (Bone nHA +NPK nano-fertilizer at 90 day).

In principle, there was a significant increase in the heights of the plants with the growth period (p<0.01) signifying the effectiveness of nano-fertilizers in controlled and gradual nutrient release (Muhammad et al., 2019). The increase over the growth period can also be attributed to the nano-fertilizers having longer contact time for the nutrient uptake in study plants. Nano-fertilizers have numerous adsorption sites that can release nutrients gradually thereby boosting growth performance in plants (Joshi et al., 2018). The % height increase was not only highest for the plant grown using bone nHA + NPK but it was observed that during the growth period (30 - 90 days) of the kale plant, bone nHA + NPK (Table 4.11) showed significantly higher kale heights (cm) of (31.00±1.53 at 30 days, 69.67±3.48 at 60 days and 97.33±1.45 at 90 days) in comparison to all other treatments. The % height increase for treatments with nano-fertilizer treatments ranged from 104.86 to 158.29 %. (Appendix II). The significantly higher plant heights signify effectiveness of bone nanofertilizers in improved growth performance of study crops. The spinach heights were shorter than those of kales due to its genotypic nature while the bean gave the highest heights due to genotypic nature of rose cocoa. Synthetic nanofertilizers had signiﬁcantly lower and similar spinach heights than bone because they have lower active adsorption sites for gradual release of nutrients.

The effectiveness of the bone nHA + NPK in improving kale height growth performance was further observed when comparing the bone nHA + NPK treatment with commercial fertilizers. The bone nHA alone had significantly higher growth performance than the Syn nHA (p<0.01). This is attributed to bone having higher stability, higher number of adsorption sites and larger surface area for adsorption and gradual release of nutrients thereby improving growth performance (Joshi et al., 2018). The bone nHA nano-fertilizers gradually release the nutrients to the plant depending on the need. Hence this reduces nutrient losses to other pathways which guarantees higher and sustainable plant growth performance.

For instance, several studies have employed nano-fertilizers to improve growth performance of plants height, dry weight biomass, crop yield, number of leaves and root elongation (Sun et al., 2020; Muhammad et al., 2019; Raliya et al., 2015). For instance, Raliya et al.(2015) working with TiO2 nanoparticle foliar application on Cyamopsis Tetragonoloba of 10 mg/L within 6 weeks and recorded higher plant height, dry weight biomass and nutrient uptake. This result agrees with those posted by other researchers (Joshi et al., 2018; Disfani et al., 2017 and Lee et al., 2012).

### 4.5.2 Dry Weight, Leaf Diameter and Plant Number of Leaves

The dry weight, leaf diameter and number of leaves of kales, spinach and beans grown using Synthetic and bone hydroxyapatite nano-fertilizers at 90 days are presented for kale (Tables 4.14), spinach (Table 4.15) and beans (Table 4.16).

#### Table 4.14: The 90 day dry weight, leaf diameter and number of leaves in kales grown using nano-fertilizers

| TREATMENT | [Kale growth parameters] Mean± SD n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | Height (cm) | L. Diameter (mm) | Dry weight (g) | No. leaves |
| Bone nHA | 88.00±2.65e | 23.00±1.15c | 150.00±1.73e | 28.00±1.15d |
| Syn nHA | 83.67±3.18d | 20.00±1.00b | 145.00±1.53d | 24.00±0.58c |
| Bone nHA +DAP | 87.67±1.76e | 21.00±0.58c | 151.33±1.20e | 28.67±1.20d |
| Syn nHA +DAP | 83.67±0.88d | 18.67±0.88b | 141.33±0.88cd | 24.33±1.20c |
| Bone nHA+ NPK | 104.33±1.45g | 21.33±1.45c | 154.00±1.53f | 29.33±1.45d |
| Syn nHA+ NPK | 93.00±1.15f | 19.00±0.58b | 145.33±6.36d | 23.00±0.58c |
| Bone nHA+DAP+NPK | 88.00±1.53d | 21.00±1.53c | 152.67±1.45d | 28.67±0.88d |
| Syn nHA+DAP+NPK | 70.33±0.88c | 19.00±0.58b | 137.33±2.19c | 21.67±1.20c |
| DAP | 46.00±1.73b | 13.33±0.33a | 121.33±2.40b | 18.33±0.88b |
| NPK | 44.67±1.86b | 13.33±1.20a | 122.00±4.04b | 17.67±0.88b |
| DAP+NPK | 46.67±1.45b | 12.33±1.20a | 120.33±2.19b | 18.00±1.15b |
| Non-treated control | 33.00±1.15a | 11.00±0.58a | 96.67±2.33a | 12.67±0.88a |
|  |  |  | P-value˂0.01 |  |

Means ± SD superscripted with similar small letters within the same column are not significantly different at p =0.05 (Anova).

#### Table 4.15: The 90 day dry weight, leaf diameter, number of pods and number of leaves in beans grown using nano-fertilizers

| TREATMENT | [Bean growth parameters] Mean± SD n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | No. Pods | L. Diameter (mm) | Dry weight (g) | No. leaves |
| Bone nHA | 28.67±0.67cd | 12.07±0.09c | 92.00±1.15c | 86.33±1.45d |
| Syn nHA | 24.23±0.09c | 10.23±0.09c | 85.33±2.73b | 79.67±1.45cd |
| Bone nHA +DAP | 29.00±1.53d | 12.13±0.12c | 92.67±0.88c | 85.67±1.45d |
| Syn nHA +DAP | 26.27±0.09c | 10.27±0.09c | 81.33±0.33b | 76.33±3.84c |
| Bone nHA+ NPK | 29.67±1.45cd | 12.3±0.12c | 93.00±1.53d | 86.00±1.53d |
| Syn nHA+ NPK | 26.03±0.07c | 10.03±0.07c | 83.67±1.86b | 78.00±1.53c |
| Bone nHA+DAP+NPK | 31.00±0.58de | 12.37±0.09c | 97.33±0.88e | 90.00±1.73e |  |
| Syn nHA+DAP+NPK | 27.47±0.09c | 10.47±0.09c | 91.67±0.88c | 80.33±0.88d |  |
| DAP | 8.27±0.12b | 8.27±0.12b | 80.33±0.88b | 70.33±1.20b |  |
| NPK | 8.53±0.07b | 8.53±0.07b | 79.33±2.03b | 67.67±0.88b |
| DAP+NPK | 8.07±0.09b | 8.07±0.09b | 77.00±1.53b | 68.00±1.53b |
| Non-treated control | 2.3±0.06a | 4.3±0.06a | 38.33±2.33a | 20.33±1.45a |
|  |  |  | P-value˂0.01 |  |

Means ± SD superscripted with similar small letters within the same column not significantly different at p =0.05 (Anova).

#### Table 4.16: The 90 day dry weight, leaf diameter and number of leaves in spinach grown using nano-fertilizers

| TREATMENT | [Spinach growth parameters] Mean± SD n=9 |  |  |  |
| --- | --- | --- | --- | --- |
|  | Height (cm) | L. Diameter (mm) | Dry weight (g) | No. leaves |
| Bone nHA | 44.67±1.76d | 14.70±0.1c | 76.67±2.33d | 16.00±0.58C |
| Syn nHA | 40.00±0.58d | 10.63±0.30b | 70.00±1.53c | 14.33±0.67c |
| Bone nHA +DAP | 43.33±1.45d | 14.37±0.24c | 77.67±1.20d | 17.67±0.88cd |
| Syn nHA +DAP | 40.67±1.76d | 14.2±0.23c | 71.33±1.76c | 16.00±0.58c |
| Bone nHA+ NPK | 49.33±1.20e | 14.67±0.45c | 76.67±2.33d | 16.00±1.53c |
| Syn nHA+ NPK | 33.00±1.15c | 14.33±0.24c | 69.67±0.88c | 16.00±0.58c |
| Bone nHA+DAP+NPK | 45.00±1.15de | 15.3±0.32c | 76.00±1.73d | 17.00±0.58cd |
| Syn nHA+DAP+NPK | 30.00±0.58c | 14.27±0.23c | 73.67±1.20c | 15.00±0.58c |
| DAP | 24.00±1.15b | 10.77±0.12b | 63.67±2.91b | 9.67±0.67a |
| NPK | 29.33±0.88c | 10.8±0.31b | 65..33±2.33b | 10.67±0.88ab |
| DAP+NPK | 28.33±1.20c | 14.53±0.24c | 62.67±0.88b | 11.33±0.33b |
| Non-treated control | 20.00±0.58a | 5.73±0.24a | 56±1.73a | 7.33±1.20a |
|  |  |  | P-value˂0.01 |  |

Means ± SD superscripted with similar small letters within the same column are not significantly different at p =0.05 (Anova).

The mean of dry weight, leaf diameter and number of leaves of kale grown in soils treated with Syn nHA, Bone nHA nano-fertilizers and their DAP/NPK combinations (Table 4.16) ranged from 18.67±0.88 to 23.00±1.15 mm (leaf diameter), 137.33±2.19 to 150.00±1.73 g (dry weight biomass), 21.67±1.20 to 28.33±1.45 (number of leaves). For spinach, (Table 4.14) it ranged from 10.63±0.30 to 14.67±0.45 mm (leaf diameter), 69.67±0.88 to 77.67±1.20 g (dry weight biomass), 14.33±0.67 to 17.67±0.88 (number of leaves). For the beans (Table 4.15) it ranged from 24.23±0.09 to 31.00±0.58 (number of pods), 10.03±0.07 to 12.37±0.09 mm (leaf diameter), 81.33±0.33 to 97.33±0.88 g (dry weight biomass), 76.33±3.84 to 90.00±1.73 (number of leaves). The effectiveness of the bone nHA in improving bean height growth performance was further observed when comparing the bone nHA treatment with that of its combination with commercial fertilizers at 90th day having statistically similar growth parameters, the bone nHA had significantly higher bean heights (p<0.01).

The bone nHA had a significantly higher leaf diameter, number of leaves and dry biomass than the Syn nHA (p<0.01). At 90 days for example, the kale dry weights were significantly higher at 150.00±1.73 g for bone nHA than that of 145.00±1.53 g of Syn nHA. Hence encapsulation of the nanoparticles with commercial fertilizers makes them to have a more selective adsorption of nutrients, enabling the gradual and controlled release of nutrients to the plants. This lengthens availability of these nutrients to the plants up to 90th maturity day to guarantee higher productivity.

Several other studies have reported use of nano-fertilizers to improve growth performance. The related findings found that seed treated with nano-Fullerenes to increase bitter melon growth parameters such as number of fruits, fruit diameter, and fruit yield biomass by 128 %, 89 % and 56 % respectively (Giraldo et al., 2014; Kole et al., 2013). Similarly, titanium (IV) oxide nanoparticles and carbon nanoparticles encapsulated with commercial fertilizer enhanced growth of mung bean (Vigra radiate L.) and increased grain yields of soybean by 19 %, by Raliya et al., 2015 and Prasad et al., 2012 respectively. Similarly, in other studies, there was an increase of 10.69 % of dry matter content in soy bean leaves and 51.5 % in the number of leaves when ZnO nanoparticles were used by Dwivedi et al.(2016).

## 4.6 Effects of Experimental Conditions on Adsorption of Metal

The adsorption of the Cd2+ and Pb2+ from their aqueous metal solution using hydroxyapatite (HA) nanofertilizers investigated factor like effects of pH, adsorbent dosage, initial metal ion concentration and time of contact with adsorption of Cd2+ and Pb2+ onto nano-fertilizers.

### 4.6.1 Effect of Initial pH on Removal of Metal ion by Nanofertilizers

The adsorption of Cd and Pb onto the nano-fertilizers was studied at a range of different pH values varying from 2 to 12 for bone nHA and synthetic nHA. The results showed that the maximum Cd adsorption occurred at pH 6 and optimal Pb adsorption occurred at pH 5. At pH lower than 4, Cd2+ adsorption reduces due to protonation of the nanofertilizer surface, hence H+ ions from the acidic surface compete with the positively charged Cd2+ thus inhibiting the adsorption process. But, at higher pH range between 6 and 7, the H+ ions concentration from the adsorption surface decreases, hence favoring the adsorption of Cd2+ onto the negatively charged bone nHA and synthetic nHA adsorbent surface. Related results have been reported elsewhere by Hameed et al. (2017).

##### Figure 4.7: pH change and the adsorption of Cd2+ and Pb2+ on bone nHA

### 4.6.2 Effect of Nano-adsorbent Dose on Removal of Metal by Nanofertilizers

Effect of nano-adsorbent dose of nano-fertilizers was established using varied dose of 0.05 to 0.5 g nano-fertilizers in 50 ml test solution of Cd2+ or Pb2+ with optimal experimental initial metal concentration of 50 µg/g and pH of 6. The results (Fig. 4.10) indicated that the amount of Cd and Pb adsorbed increased with increase in the nano-adsorbent dose as shown on the graph. This can be attributed to increase in the number of exposed adsorption sites favoring the adsorption process of the metals.

##### Figure 4.8: Adsorbent dosage on Pb2+ adsorption using bone nHA

However, for the Cd adsorption the amount adsorbed decreased after certain point (shown on Fig 4.10), due to overlapping of the active adsorption sites thereby decreasing the overall adsorption exposed surface area available to Cd2+ adsorption (Zhangwei et al. 2019; Bertazzo et al. 2010). It was found that 5 g/L of nano-fertilizers adsorbed 99 % of 50 mg/L of Cd. But for Pb at 4g/L adsorbent dosage, the adsorption process remained constant.

### 4.6.3 Effect of Initial Metal Concentration on Adsorption by Nanofertilizers

The initial heavy metal concentrations effect was investigated at pH 6, 5g/L dosage for both the Cd and Pb by variation of respective heavy metal concentrations as follows; 5, 10, 15, 25, 50, 100, 250 and 500 mg/L at room temperature (300 K). The result presented in Fig. 4.11 indicated that the amount adsorbed decreased with the increase in the initial metal concentrations of both the Cd2+ and Pb2+ (Qi et al., 2020; Nilwala et al., 2011). This can be attributed to presence of scarce adsorption sites to adsorb the increasing number of Cd2+ or Pb2+ ions as the initial concentration is being increased.

##### Figure 4.9: Effect of Initial metal concentration on removal of Cd2+ and Pb2+ on bone nHA

### 4.6.4 Effect of Contact Time on Adsorption of Metal by Nanofertilizers

Results on effect of time of contact on Cd2+ and Pb2+ adsorption by nanofertilizers using the same initial metal ion concentration (50 µg/ml) at pH 6 and 5g/L nanofertilizer dosage as other adsorption experiments, was found to have related kinetic properties. Time was varied between 0 to 240 minutes. The results presented on Figure 4.12 shows that for both metal ions, adsorption is optimal at 120 minutes. The faster adsorption observed with bone nHA, is attributed to higher stable adsorption sites in nanohydroxyapatites and higher adsorption efficiency of heavy metal in the nanofertilizers (Lateef et al., 2016).

##### Figure 4.10: Contact time on the adsorption of Cd2+ and Pb2+ on bone nHA

## 4.7 Adsorption Isotherms after Optimization

This study on the adsorption process of Cd2+ and Pb2+ from their aqueous solutions using bone nanofertilizers, studied the factors that affects adsorption like pH, contact time, initial concentration and nano-adsorbent dose (Shojaei et al., 2019).

Langmuir and Freundlich isotherm Equations (2.2 and 2.3) were fitted with experimental data obtained for Cd2+ and Pb2+ions against initial metal concentration for bone and synthetic nDAP, nNPK, nNPK-DAP, nHA nano-fertilizers. The constants of Qmax (adsorptive capacity (mg/g) and b (binding energy to adsorption sites) were obtained from the Langmuir equation linear plot of 1/qe against 1/Ce as slope and y-intercept respectively. For Freundlich, Kf and l/n (y-intercept and gradient respectively) were computed from a linear plot of log qe, against log Ce. qe (maximum adsorptive capacity (mg/g), Kf (Freundlich constant on affinity to adsorption) and ‘n’(adsorptive intensity). The results are discussed in the following subsections.

## 4.8 Adsorption Isotherms Fitting for Cadmium and Lead

### 4.8.1 Adsorption Isotherms Fitting for Cadmium

Table 4.17 shows the Langmuir and Freundlich isotherms adsorption parameters for Cd2+ using nano-fertilizers which was done using the batch experiment.

#### Table 4.17: Langmuir and Freundlich Cd2+adsorption isotherm parameter models

|  | Langmuir parameters |  |  |  | Freundlich Parameters |  |  |  |  | Best model |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ADSORBENT |  | Qmax | b | R2 |  | 1/n | n | Kf | R2 |  |  |  |
| Bone nHA |  | 62.5 | 1.778 | 0.997 |  | 0.540 | 1.852 | 0.1720 | 0.940 |  | Langmuir |  |
| Syn nHA |  | 43.48 | 3.830 | 0.996 |  | 0.539 | 1.855 | 0.1723 | 0.946 |  | Langmuir |  |
| Bone nHA +DAP |  | 58.82 | 1.889 | 0.997 |  | 0.531 | 1.883 | 0.1746 | 0.943 |  | Langmuir |  |
| Syn nHA +DAP |  | 50.00 | 2.857 | 0.997 |  | 0.512 | 1.953 | 0.1749 | 0.949 |  | Langmuir |  |
| Bone nHA+ NPK |  | 55.55 | 2.250 | 0.997 |  | 0.534 | 1.873 | 0.1726 | 0.948 |  | Langmuir |  |
| Syn nHA+ NPK |  | 50.00 | 2.860 | 0.997 |  | 0.508 | 1.967 | 0.1752 | 0.941 |  | Langmuir |  |
| Bone nHA+DAP+NPK |  | 52.63 | 2.111 | 0.991 |  | 0.657 | 1.5221 | 0.1652 | 0.948 |  | Langmuir |  |
| Syn nHA+DAP+NPK |  | 45.45 | 3.667 | 0.991 |  | 0.506 | 1.976 | 0.1746 | 0.944 |  | Langmuir |  |

Results for Langmuir isotherms indicate that there was correlation in Cd adsorption because R2 > 0.996 except for bone nHA+DAP+NPK while in Freundlich isotherms had no correlation because R2 ˂ 0.95. The results show that the adsorption of Cd2+onto bone and synthetic nano-fertilizers, for nDAP, nNPK, nDAP-NPK fitted very well in Langmuir isotherm model. Adsorption capacities for the bone nano-fertilizers adsorbents were higher than those of the synthetic nano-fertilizer adsorbents. This explains why bone nanofertilizers have a higher efficacy in reducing Cd uptake in study plants. The ‘b’ values were higher in synthetic nHA with 3.83 while the bone nHA had lower ‘b’ value of 2.857. Therefore their affinity to adsorption sites and measure of absorptive energy needed, which was lower for bone made nano-fertilizers than synthetic counter parts, hence making adsorption to it more favorable (Montazeri et al., 2010). This indicates that the bone nano-fertilizers have higher ability to adsorb and immobilize Cd2+ thereby reducing its uptake in kale, spinach and bean plants. The Qmax parameter indicates the bone made nano-fertilizers have higher capacity to adsorb and immobilize cadmium as compared to synthetic nano-fertilizers. For instance synthetic nHA had Qmax value of 43.48 mg g-1 while bone nHA had Qmax value for Cd2+ adsorption of 62.25 mg g-1.

### 4.8.2 Adsorption Isotherms Fitting for Lead

Table 4.18 shows the Langmuir and Freundlich isotherms adsorption parameters for Pb2+ using nano-fertilizers which was done using the batch experiment.

#### Table 4.18: Results of Langmuir and Freundlich adsorption isotherm parameter model for Pb2+

|  | Langmuir parameters |  |  | Freundlich Parameters |  |  |  |  | Best model |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ADSORBENT | Qmax | b | R2 |  | 1/n | N | Kf | R2 |  |  |  |
| Bone nHA | 55.55 | 2.250 | 0.944 |  | 0.680 | 1.4706 | 0.1889 | 0.997 |  | Freundlich |  |
| Syn nHA | 43.47 | 3.840 | 0.949 |  | 0.836 | 1.1962 | 0.1623 | 0.996 |  | Freundlich |  |
| Bone nHA +DAP | 58.83 | 1.888 | 0.942 |  | 0.667 | 1.4993 | 0.1682 | 0.997 |  | Freundlich |  |
| Syn nHA +DAP | 50.00 | 2.857 | 0.941 |  | 0.606 | 1.6500 | 0.1610 | 0.998 |  | Freundlich |  |
| Bone nHA+ NPK | 55.56 | 2.249 | 0.943 |  | 0.619 | 1.6155 | 0.1652 | 0.997 |  | Freundlich |  |
| Syn nHA+ NPK | 52.63 | 2.111 | 0.941 |  | 0.657 | 1.5221 | 0.1626 | 0.998 |  | Freundlich |  |
| Bone nHA+DAP+NPK | 58.82 | 1.889 | 0.943 |  | 0.836 | 1.1962 | 0.1889 | 0.997 |  | Freundlich |  |
| Syn nHA+DAP+NPK | 50.00 | 2.860 | 0.941 |  | 0.607 | 1.6474 | 0.1635 | 0.997 |  | Freundlich |  |

The above results on the adsorption of Pb2+ onto bone and synthetic nano-fertilizers, fitted well in Freundlich isotherm model as it posts higher coefficient of correlation (R2 > 0.996) than the Langmuir model which posted correlation coefficient (R2 ˂ 0.95). When 1/n ˂ 1, it indicates that the adsorption process of Pb is favorable. However in bone nano-fertilizers, ‘1/n’ value is lower than in synthetic nano-fertilizers, signifying the adsorption process is more favorable in bone nanofertilizers due to more stable adsorption sites and chelation sites than synthetic nano-fertilizers. Similarly the Kf value are higher in bone nanofertilizers than in the synthetic nanofertilizers implying the adsorption process of Pb is more favorable in the bone nanofertilizers (Ling et al., 2017; Liu & Lal, 2014).

## 4.9 Adsorption Kinetic Studies

Kinetics of adsorption Cd2+ and Pb2+ was investigated using pseudo 1st order and pseudo 2nd order model equations to explain the adsorption rate and adsorptive capacity of the nanofertilizers. Linear plots of Equation 2.4 and 2.5 were applied to determine the best fit model and compute kinetic parameters. The calculated constants of Qe of pseudo 1st order and Qe of pseudo 2nd order models are compared to the experimental Qe calculated using Equation 2.4 and Equation 2.5 data obtained as described in Section 2.8.2. Similarly, the rates of adsorption K1 and K2 values were also calculated and obtained from graphical plots of pseudo 1st order and pseudo 2nd order models.

### 4.9.1 Adsorption Kinetic Studies for Cadmium and Lead

Kinetic constants of pseudo 1st order and pseudo 2nd order equations for cadmium in all the nano-fertilizers are recorded in Table 4.19 and Table 4.20.

#### Table 4.19: Computed results of adsorption kinetic using pseudo first order equation

| ADSORBENT |  | Cd2+ kinetic parameters |  |  |  | Pb2+ kinetic parameters |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | K1 | Qe | R2 |  | K1 | Qe | R2 |
| Bone nHA | 0.00304 | 0.707 | 0.999 |  | 0.00260 | 1.036 | 0.904 |
| Syn nHA | 0.00304 | 0.701 | 0.999 |  | 0.002605 | 0.991 | 0.903 |
| Bone nHA +DAP | 0.00217 | 1.823 | 0.999 |  | 0.00261 | 1.051 | 0.901 |
| Syn nHA +DAP | 0.003041 | 0.703 | 0.998 |  | 0.00261 | 0.928 | 0.914 |
| Bone nHA+ NPK | 0.00261 | 0.8124 | 0.999 |  | 0.00304 | 0.693 | 0.928 |
| Syn nHA+ NPK | 0.002605 | 0.724 | 0.999 |  | 0.00259 | 0.963 | 0.909 |
| Bone nHA+DAP+NPK | 0.002715 | 0.951 | 0.998 |  | 0.002939 | 0.7592 | 0.927 |
| Syn nHA+DAP+NPK | 0.002605 | 0.982 | 0.997 |  | 0.003039 | 0.7496 | 0.918 |

The pseudo 1st order and the pseudo 2nd order adsorption models were used to explain on the adsorption kinetics mechanisms of the nano-fertilizer adsorbents. The coefficient of correlation (R2 values) were obtained from these linear plots and the figures for Cd adsorption indicate R2 > 0.995, signifying a better fit than Pb whose R2 ˂ 0.95 (Table 4.17). The results also indicated that bone nanofertilizers had higher adsorption capacity (Qe) values than the synthetic nanofertilizers. Also the pseudo 1st order constant (K1) values were lower in bone nanofertilizers than synthetic nanofertilizers. This explains why bone nanofertilizers have higher adsorption efficiency than synthetic nanofertilizers.

The results for pseudo second order equation parameters K2, Qe and R2, for all the eight treatments were calculated and recorded in Table 4.20.

#### Table 4.20: Second order pseudo kinetic parameters

| ADSORBENT |  | Cd2+ kinetic parameters |  |  | Pb2+ kinetic parameters |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | K1 | Qe | R2 | K1 | Qe | R2 |
| Bone nHA | 0.00446 | 30.30 | 0.928 | 0.004289 | 31.15 | 0.999 |
| Syn nHA | 0.00437 | 30.21 | 0.928 | 0.00314 | 30.12 | 0.999 |
| Bone nHA +DAP | 0.00333 | 31.25 | 0.848 | 0.006184 | 29.41 | 0.998 |
| Syn nHA +DAP | 0.00588 | 29.16 | 0.928 | 0.005902 | 29.33 | 0.997 |
| Bone nHA+ NPK | 0.005902 | 29.33 | 0.923 | 0.005448 | 30.21 | 0.999 |
| Syn nHA+ NPK | 0.00537 | 29.24 | 0.927 | 0.004472 | 29.15 | 0.996 |
| Bone nHA+DAP+NPK | 0.002989 | 31.15 | 0.921 | 0.00606 | 29.24 | 0.998 |
| Syn nHA+DAP+NPK | 0.002878 | 30.85 | 0.910 | 0.00601 | 29.12 | 0.997 |

Table 4.20 indicates that the Pseudo 2nd order model is best fitted to explain Pb2+ ions adsorption by the nano-fertilizer adsorbents. This is because the Pseudo second order models recorded R2> 0.995 while those of Cd are R2 ˂ 0.95.in all the nano-fertilizer experiments. Secondly, the results indicate that bone nanofertilizers had higher adsorption capacity (Qe) values than the synthetic nanofertilizers. This explains why bone nanofertilizers have significantly higher adsorption efficiency (p˂0.001) than synthetic nanofertilizers. The Pseudo second model depicts that the adsorption process was heterogeneous and multi-layered (Wu et al., 2012; Bertazzo et al., 2010). Though both Cd and Pb are transition metals, Cd is lighter than Pb, that’s why they conform to different adsorption isotherms.

## 4.10 Nutrient Release Concentration Studies

Nitrate, phosphate and potassium nutrient release patterns of the bone nanofertilizers was investigated by using experimental soil mixed with nanofertilizers at 10 % (w/w) and then packed in a column. The Tables 4.21, 4.22 and 4.23 below shows results for the amount of nitrate, phosphate and potassium nutrients released after every 5 days upto 40 days respectively.

#### Table 4.21: Nitrate nutrient release concentrations by nano-fertilizers and commercial fertilizers

| Days of Elution | Released Nitrate (NO3-) concentration Mean± SD (µgg-1) n=9 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Bone nHA | Bone nHA+ DAP | Bone nHA+ NPK | Synthetic nHA | Synthetic nHA+ DAP | Synthetic nHA+ NPK | DAP | NPK |
| Day 5 Day 10 | 73.45±0.36eA 48.57±0.22g A | 89.67±0.18e C 51.52±0.17d B | 89.72±0.16eC 55.02±0.20dC | 74.33±0.27eA 48.62±0.20dA | 95.2±0.70fD 51.66±0.22eB | 84.74±0.15fB 47.29±0.10eA | 162.62±0.79hE 98.04±0.14gD | 165.5±1.23hE 101.01±0.11gE |
| Day 15 | 39.32±0.94d A | 37.91±0.18c A | 39.36±0.85aC | 39.57±0.68cA | 41.33±0.24dB | 39.40±0.14dA | 61.92±0.28fC | 67.34±0.92fD |
| Day 20 | 36.49±0.19b A | 34.13±0.04b A | 35.81±0.59bA | 38.61±0.57cB | 38.51±0.21cdB | 37.29±0.14cdA | 49.0±0.96eC | 49.21±1.13eC |
| Day 25 | 34.31±0.73b B | 33.84±0.12b B | 34.36±0.49bB | 34.22±0.12bB | 35.43±1.07cBC | 34.89±0.14cA | 29.54±0.51dA | 28.67±0.19dA |
| Day 30 | 31.97±1.12a B | 32.47±0.73bB | 30.73±0.07aB | 30.68±1.66aB | 32.19±0.17bB | 31.58±0.13bB | 15.48±0.73cA | 15.54±0.49cA |
| Day 35 | 30.02±0.10a B | 30.56±0.31bcA | 29.34±0.33aB | 28.96±0.22aB | 29.56±0.99aB | 29.06±0.11aB | 11.24±0.62bA | 10.34±0.85bA |
| Day 40 | 29.98±0.08a B | 29.28±1.10aB | 29.11±0.42aB | 28.03±0.40aB | 29.49±1.02aB | 28.81±0.10aB | 9.18±0.11aA | 8.98±1.03Aa |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

#### Table 4.22: Phosphate nutrient release concentrations by nano-fertilizers and commercial fertilizers

| Days of Elution | Released Phosphate (PO43-) concentration Mean± SD (µgg-1) n=9 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Bone nHA | Bone nHA+ DAP | Bone nHA+ NPK | Synthetic nHA | Synthetic nHA+ DAP | Synthetic nHA+ NPK | DAP | NPK |
| Day 5 Day 10 | 36.45±0.33e A 24.57±0.19gA | 44.67±0.15e B 25.52±0.14dA | 44.72±0.13eB 28.02±0.17dB | 37.33±0.24eA 24.62±0.18dA | 47.20±0.67fC 25.66±0.19eA | 42.74±0.12fB 23.29±0.10eA | 80.62±0.76hD 48.04±0.11gC | 82.50±1.20hD 50.01±0.11gC |
| Day 15 | 20.32±0.92dA | 18.91±0.16c A | 20.36±0.83cA | 19.57±0.66cA | 20.33±0.22dA | 19.40±0.12dA | 29.92±0.26fB | 33.34±0.90fC |
| Day 20 | 19.49±0.18bA | 17.13±0.02bA | 18.81±0.57bA | 17.61±0.55cA | 19.51±0.19cdA | 18.29±0.12cdA | 23.00±0.94eB | 24.21±1.11eB |
| Day 25 | 17.31±0.72bB | 16.84±0.11b B | 17.36±0.49bB | 16.22±0.10bB | 17.43±1.06cB | 17.89±0.12cB | 14.54±0.50dA | 14.67±0.19dA |
| Day 30 | 16.97±1.11aB | 15.47±0.71bB | 15.73±0.07aB | 15.68±1.65aB | 16.19±0.16bB | 15.58±0.12bB | 7.48±0.72cA | 8.54±0.49cA |
| Day 35 | 15.02±0.10a B | 14.56±0.32aB | 14.34±0.34aB | 14.96±0.23aB | 14.56±0.99aB | 14.06±0.12aB | 6.24±0.63bA | 5.34±0.86bA |
| Day 40 | 14.98±0.09aB | 13.28±1.12aB | 14.11±0.44aB | 13.93±0.41aB | 14.49±1.03aB | 13.81±0.12aB | 5.38±0.14aA | 5.08±1.07aA |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

#### Table 4.23: Potassium nutrient release concentrations by nano-fertilizers and conventional fertilizers

| Days of Elution | Released Potassium (K+) concentration Mean± SD (µgg-1) n=9 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Bone nHA | Bone nHA+ DAP | Bone nHA+ NPK | Synthetic nHA | Synthetic nHA+ DAP | Synthetic nHA+ NPK | DAP | NPK |
| Day 5 Day 10 | 39.45±0.35eA 26.47±0.19gA | 46.67±0.14eB 28.52±0.14dB | 46.72±0.12eB 30.02±0.18dB | 38.33±0.22eA 25.62±0.38dA | 45.2±0.65fB 26.56±0.19eA | 45.74±0.16fB 26.89±0.10eA | 81.62±0.66hC 49.04±0.12gC | 84.5±1.22hC 53.01±0.21gD |
| Day 15 | 21.32±0.92dA | 20.91±0.26cA | 22.36±0.73cB | 20.57±0.65cA | 21.73±0.23dA | 22.46±0.18dB | 30.92±0.27fC | 35.34±0.92fD |
| Day 20 | 20.49±0.19bB | 18.13±0.02bA | 20.81±0.56bB | 18.61±0.56cA | 19.91±0.17cdA | 19.29±0.13cdA | 24.11±0.95eC | 25.21±1.11eC |
| Day 25 | 19.31±0.71bD | 17.84±0.11bB | 19.36±0.48bB | 17.22±0.11bB | 18.43±1.05cC | 18.89±0.13cC | 15.54±0.51dA | 16.67±0.19dA |
| Day 30 | 18.97±1.13aD | 17.47±0.71bC | 17.73±0.08aC | 16.68±1.66aB | 17.19±0.17bC | 17.58±0.13bC | 8.48±0.73cA | 9.54±0.48cA |
| Day 35 | 16.92±0.10aC | 16.56±0.32aC | 16.94±0.34aC | 15.96±0.23aC | 16.56±0.99aC | 15.06±0.12aC | 7.24±0.63bB | 6.34±0.86aB |
| Day 40 | 15.78±0.08aC | 16.28±1.11aD | 16.71±0.43aD | 15.63±0.44aC | 15.49±1.02aC | 14.81±0.11aB | 6.08±0.13aA | 5.88±1.06aA |

Means ± SD superscripted with similar small letters within the same column and similar capital letters within the same row are not significantly different at p =0.05 (Anova).

Nutrient release concentrations of commercial fertilizers and nano-fertilizer treatments are presented in Table 4.21, Table 4.22 and Table 4.23. A typical example is the account that the total nutrient released for bone nHA and synthetic nHA at 40th day is 320 and 319 ug/g respectively. The rest of the nutrients in nanofertilizers remain to be released as plants head towards maturity. Bone nanofertilizers and its encapsulated nanofertilizers had significantly (p˂0.05) lower and better controlled nitrate, phosphate and potassium nutrient release rate than synthetic nanofertilizer and its encapsulations. This is attributed to bone nanofertilizers having higher number of adsorption sites for increased contact surface area to volume ratio thereby enhancing controlled and sustainable nutrients release to the crop when needed.

On the other hand nutrient release experiment for the commercial fertilizers displayed significantly rapid nitrate, phosphate and potassium nutrient release rates and then decreased gradually with time (Fig 4.15). A good scenario is the fact that the total nutrient released for commercial DAP and NPK at 40th day is 437 and 443 ug/g. This leads to exhaustion of the nutrients to support higher crop productivity as crops nears maturity (Nilwala et al., 2011). This can be attributed to lack of adequate adsorption sites in commercial fertilizers for gradual and sustainable release of nitrate, phosphate and potassium nutrients. The comparison between commercial fertilizers and nano-fertilizers shows that the release concentrations of two categories of fertilizer had a significant difference (p˂0.01), which indicated that the nano-fertilizer had more effect of regulating the nitrate release rate. Results concur with those obtained by Cai et al. (2014). The trend exhibited in nitrate nutrient release rate is shown by graphical representation below.

##### Figure 4.11: Graph on NO3- released by Bone nHA nanofertilizers within 40 days

##### Figure 4.12: Graph on NO3-- release by synthetic nHA nanofertilizers within 40 days

##### Figure 4.13: Graph on NO3- release by commercial fertilizers within 40 days

This indicates that the bone nano-fertilizers have a higher impact in regulating and having a more controlled gradual release of nitrate nutrients since they have a higher number of adsorption sites in comparison with synthetic nanofertilizers (Nilwala et al., 2011). However the phosphate release rates of the treatments are relatively lower than nitrate release rates (Table 4.22). This is attributed to poor mobility of P adsorbed by experimental soil. There was gradual decrease in phosphate release rate in nano-fertilizer with increasing length of elution time.

For the potassium, the nano-fertilizer had more controlled release on K+. Generally, the release concentrations of K+ were much slower than that of nitrates in each sampling and faster than that of phosphates. Forces that trigger release rate mechanisms are like van der waals forces and hydrogen bonding. The difference in nutrient release rate variation can also be attributed to several factors such as nature of nutrient, adsorption, and fixation power of adsorbent to various nutrient ions (Liu & Lal, 2014).

# CHAPTER FIVE

# CONCLUSIONS AND RECOMMENDATIONS

## 5.1 Conclusions

Based on the results obtained in this study, following key conclusions can be made.

- Bone nHA nano-fertilizers and its encapsulations had smaller crystallite size than synthetic nanofertilizers.

- Bone nHA nano-fertilizers and its encapsulations had higher reduction of Cd and Pb in beans, spinach and kale leaves grown than synthetic nHA encapsulations over the 90 days.

- Bone nHA nano-fertilizers had more increased growth performance parameter than syn nHA; plant height, leaf diameter, plant number of leaves, stem diameter and bean number of pods in greenhouse grown kale, spinach, and beans. However bone nHA nanofertilizers and its encapsulations had the highest improvement in growth performance of the plants grown within 90 days.

- Bone nHA nano-fertilizers had higher adsorption capacity than synthetic nHA. Cd adsorption fitted well in Langmuir while Pb adsorption fitted better with Freundlich isotherms. The Cd fitted well with pseudo 1st order while Pb fitted well in second-order kinetics model.

- Bone nHA nano-fertilizers and its encapsulations had a slower controlled nutrient release rate of NO3-, PO43- and K+ nutrients than synthetic nHA nano-fertilizers.

- Bone nHA is the best treatment in reducing Cd and Pb uptake, regulating nutrient release rate and in improving growth performance parameters. Hence it can be used alone in the growing of kales, spinach and beans in Cd/Pb polluted soils.

### 5.2.1 Recommendations from the Study

- Bone nano-fertilizer can be possibly be used in growing of kales, spinach and beans in Cd/Pb medially polluted soils, as well as it be used for the gradual release of NO3-, PO43- and K+ nutrients.

- Promote the use of bone nHA nano-fertilizer which has been shown to significantly increase in growth performance in kale, spinach and beans.

### 5.2.2 Recommendation for Further Research

- Bone nanofertilizers adsorption mechanism of other heavy metals to be studied.

- Study of effect of bone nanofertilizers on growth performance, heavy metal and nutrient uptake by other crops should be done.

- Study on the effect of bone nanofertilizers on bioavailability of essential nutrients in study crops should be done.

# REFERENCES

Abbas, T., Rizwan, M., Zia-Ur-Rehman, M., Qayyum, M. F., Abbas, F., Ali, S., Hannan, F., Rinklebe, J. and Ok, Y. S. (2017). Effect of biochar on cadmium bioavailability and uptake in wheat (Triticum aestivum L.) grown in a soil with aged contamination. Ecotoxicological Environmental Safety. 140: 37–47.

Ahmed, M. M. M. (2018). Physiological studies on fertilization of flame seedlings grapevines by nano-technology system. M. Sc. Thesis Faculty of Agriculture . Minia University Egypt, 63-73.

Alexandre, K., Xiao, H., Zhiyong, Z., Yuhui, M., P. Z., Gibson, M. A. and Yukui, R. (2017). Magnetic (Fe3O4) Nanoparticles Reduce Heavy Metals Uptake and Mitigate Their Toxicity in Wheat Seedling. Sustainable Polymer Composites and Nanocomposites.23: 123–129.

Ansari, S. M., Naghib, F. and Moztarzadeh, A. S. (2011). Synthesis and characterization of nanohydroxyapatite- calcium hydroxide for dental composites. Environmental Science & Technology. 19(11): 8471 - 8483.

Asare, E. A., Zaini, B. A., Rafeah, B. W., Kwabera, D. E. and Wilson, F. (2019).Validation of the Atomic Absorption Spectroscopy (AAS) for Heavy Metal Analysis and Geochemical Exploration of sediment samples from the Sebangan River. Advances in Analytical Chemistry. 9(2): 23-33.

Banerjee, S., Yogesh, C., Sharma, K. M., Dubey, S., Kumar, R. G. and Chattopadhyaya, M. C. (2019). Adsorption Characteristics of Alumina (Al2O3) Nanoparticles for the Removal of Hazardous dye, (Orange G) from aqueous solutions. Arabian Journal of Chemistry. 12(8): 5339-5354.

Bertazzo, S., Zambuzzi, W. F., Campos, D. D. P., Ogeda, T. L., Ferreira, C. V. & Bertran, C. A. (2010). Hydroxyapatite surface solubility and effect on cell adhesion. Colloids Surface Biointerfaces.78: 177–184.

Beyer, Y., Beanland, R. and Midgley, P. A. (2012). Low Voltage STEM Imaging of Multi-walled Carbon Nanotubes. Micron.43: 428–434.

Birendra, N. B., Vijay, K. M., Shyam, B. R., Om, P. and Kumar, D. (2019). Structure of Apatite Nanoparticles Derived from Marine Animal (Crab) shells: An Environment-Friendly and cost-effective Novel Approach to Recycle Seafood Waste. ACS OMEGA. 4(7): 12753-12758.

Buyukkilic, A. Y., Malatya, T and Yunerdag, G. (2022). Heavy Metal Evaluation of Overused Commercial Fertilizers and Their Interaction with Soil Properties. Journal of Agricultural Production. 3(2): 58-68.

Cai, D. Q., Jiang, J., Wu, Z. Y., Feng, H. Y., Brown, I. G., Chu, P. K. and Yu, Z. L. (2014). Controlling Nitrogen Migration Through Micro-nano Networks. Science Reprentation.4: 36-65.

Calin, A. D., Galceran, J., Carlos, R. C., Puy, J., Encarnacio, C., Jose, S., Monne, J., Rachel, W. and Vakourov, A. (2012). Dissolution Kinetics and solubility of ZnO Nanoparticles. Journal Physical Chemistry. 10: 1021 - 1029.

Chuanjia, J., George, R. A. and Heileen, H. K. (2015). Effects of natural organic matter properties of the Dissolution kinetics of ZnO nanoparticles. Environmental Science & Technology. 49(19): 11476 - 11484.

Cui, H. X., Liu, Q., Jiang, J., Sun, C. J. and Gu, W. (2010). Applications of Nano-technology in Agrochemical Formulation, Perspectives, Challenges and Strategies. International Conference on Nanoagriculture, Sao Pedro, Brazil, 20-25 June 2010: 14–22.

Das, C. K., Srivastava, G., Dubey, A., Roy, M., Jain, S., Saxena, M , Sethy, N. K., Harke, S., Sarkar, S. and Misra, K. (2016). Nano-iron Pyrite Seed Dressing: A sustainable intervention to reduce fertilizer consumption in vegetable (beetroot, carrot), spice (fenugreek), fodder (alfalfa), and oilseed (mustard, sesamum) crops. Nanotechnology and Environmental Engineering.1: 2-6.

Davarpanah, S., Tehranifar, A., Abadia, J., Davarynejad, G. and Khorasani, R. (2016). Effects of Foliar Applications of Zinc and Boron Nanofertilizers on Pomegranate (Punicagranatum cv. Ardestani) Fruit Yield and Quality. Science Horticulture. 210: 57–65.

DeRosa, M. C., Monreal, C., Walsh, R., Schnitzer, M. R. & Sultan, Y. (2010). Nanotechnology in Fertilizers. Natural Nanotechnology. 5: 91–92.

Disfani, M. N., Mikhak, A., Kassaee, M. Z. and Maghari, A. (2017). Effects of Nano Fe/SiO2 Fertilizers on Germination and Growth of Barley and Maize. Archives Agronomy Soil Science.. 63: 817–826.

Dong, Q., Fang, J., Huang, F. and Cai, K. (2019). Silicon Amendment Reduces Soil Cd Availability and Cd Uptake of Two Pennisetum Species. International.Journal Environmental Resource in Public Health. 16: 16–24.

Du, W., Yang, J., Liang, X., Peng, Q. and Mao, H. (2019). Comparison Study of ZnO Nanoparticles and ZnSO4 on Wheat Growth: From toxicity and zinc biofortification. Chemosphere. 227: 109–116.

Dubey, A. and Mailapalli, D. R. (2016). Nanofertilisers, Nanopesticides, Nanosensors of Pest and Nanotoxicity in Agriculture. In Sustainable Agriculture Reviews; Lichtfouse, E., Ed.; Springer: Chem, Switzerland. 19: 307–330.

Dwivedi, S., Al-Khedhairy, A. A., Saquib, Q. and Musarrat, J. (2016). Understanding the Role of Nano-materials in Agriculture. In Microbial Inoculants in Sustainable Agricultural Productivity; Singh, D.P., Singh, H.B., Prabha, R., Eds.; Springer: New Delhi, India. 216:. 271–288..

El-Feky, S. A., Mohammed, M. A., Osman, Y. A., Khater, M. S. and Elsherbini, E. (2013). Effect of Magnetite Nanofertilizer on Growth and Yield of Ocimumbasilicum L. International Journal of Indigenous Medicinal Plants. 46: 1286–1293.

Ewa, B. W., Dominik, S., Patryk, O. and Anna, W. M. (2019). Effects of Titanium Dioxide (TiO2) Nanoparticles Exposure on Human Health-Review. Biological Trace Elements Research. 193: 118-129.

FAO. (2015). The State of Food Insecurity in the World: Meeting the 2015 International Hunger Targets; Taking Stock of Uneven Progress. Italy, Rome, 2015:. 36-83.

Garcia, N. C. A., Jimeneze, H. M. C., Soto, M., Blasco, J., Soto, M. and Fernandez, A. (2015). STEM-in-SEM High Resolution Imaging of Gold Nanoparticles and Bivalve Tissues in Bioaccumulation Experiments. Analysts. 140: 3082-3089.

Gil-Díaz, M., Pinilla, P. A. J. and Jath, H. M. (2017). Viability of a Nano-remediation Process in Single or Multi-metallloid Contaminated Soils. Journal of Hazardous Matererial. 321: 812–819.

Giroto, A., Fidelis, S. and Ribeiro, C. (2015). Controlled Drug Release from Hydroxyapatite Nanoparticles Incoporated into Biogradable Soluble Host matrixes. RSC Advances. 5: 104179-104186.

Giraldo, J. P., Landry, M. P., Iverson, N. M., Faltermeier, S. M., McNicholas, T. P., Boghossian, A. A., Reuel, N. F., Brew, J. A., Hilmer, A. J., Sen, F. and Strano, M. S. (2014). Plant Nanobionics Approach to Augment Photosynthesis and Biochemical Sensing. Natural Matter.10: 1038-1045.

Guangmei, T., Xiaole, L. Q., Chenjiao, W., Lei, L., Jiahang, G., Xiaolin, D., Meng, L. and Jingxin, N. (2021). Nitrogen and Phosphorus Fertilization Increases the Uptake of Soil Heavy Metal Pollutants by Plant Community. Research Square https://doi.org/10.21203/rs.3-rs-413625/v1. 10: 38-45.

Hameed, K. S., Muthirulan, P. M. M. and Sundaram, M. M. (2017). Adsorption of Chromotrope Dye by Activated Carbons Obtained from the Seeds of various Plants: Equilibrium and Kinetics Studies,. Arabic. Journal of Chemistry.10(2): 2225–2233.

Helaly, M. N., El-Metwally, M. A., El-Hoseiny, H., Omar, S. A. and El-Sheery, N. I. (2014). Effect of Nanoparticles on Biological Contamination of Invitro Cultures and Organogenic Regeneration of Bananas. Australian Journal of Crop Science. 8: 612–624.

Iqbal, M., Raja, N. I., Ejaz, M., Hussain, M. and Yasmeen, F. (2019). Effect of Silver Nanoparticles on Growth of Wheat under Heat Stress. International Journal of Science and Technology. 43: 387–395.

Janan, H., Zachary, J. O. D., Arka, R. and Kathrya, R. R. (2014). In Situ Quantification of Silver Nanoparticles: Dissolution kinetics in simulated sweep using Linear sweep stripping voltametry. Environmental Science & Technology. 53(22): 13117 - 13125.

Joshi, A., Kaur, S., Nayyar, H., Dharamvir, K. and Verma, G. (2018). Multi-walled Carbon Nanotubes Applied Through Seed-priming Influence Early Germination, Root Hair, Growth and Yield of Bread Wheat (Triticum aestivum L.). Journal of Science and Food Agriculture.98. 3148–3160.

Karthik, C., Suresh, S., Sneha, M. and Kavitha, S. (2019). The FTIR Approach of Green Synthesized Silver nanoparticles by Ocimum Sanatum and Ocimum Gratisssimum on Mung Bean Seeds. Inorganic and Nano-metal Chemistry. 50: 606-612.

Kole, C. P., Kole, K. M., Podila, P. C., Randunu, P., Choudhary, R., Ke, M. R. and Marcus, R. K. (2013). Nanobiotechnology can Boost Crop Production and Quality: First evidence from increased plant biomass, fruit yield and phytomedicine content in bitter melon (Momordica charantia). BMC Biotechnology.13(37): 1472–1550.

Konate A., R., G. M. A. and Yuang, M. (2014). Magnetic (Fe3O4) Nanoparticles Reduce Heavy Uptake and Mitigate Their Toxicity in Wheat Seedling. Sustainability. 140: 1–8.

Lateef, A., Nazir, R., Khan, M. N., Jamil, N., Alam, S., Shah, R. and Saleem, M. (2016). Synthesis and Characterization of Zeolite based Nanocomposite: An Environment Friendly Slow-release Fertilizer. Microporous Matter. 232: 174–183.

Lee, W. M., Kwak, J. I. and Ani, Y. J. (2012). Effect of Silver Nanoparticles in Crop Plants; Phaseolus Radiates and Sorghum Bicolour; Media Effect on Phytotoxicity. Chemosphere. 86: 492-499.

Ling, D., Jianbing, L., Wei, L., Q. Z. and Shahid. L. (2017). Influence of NanoHydroxyapatite on the Metal Bioavailability, Plant Metal Accumulation and Root Soil., Exudates of Ryegrass for Phytoremediation in Lead-Polluted. Journal of Biomaterials and Nanobiotechnology.34: 342–350.

Liu, R. and Lal, R. (2014). Synthetic Apatite nano-particles as a Phosphorus Fertilizer for Soy Bean (Glycine max). In Scientific Reports. 4: 18–29.

Ma, C., Chhikara, S., White, J. C., Xing, B., Musante, C. and Dhankher, O. P. (2013). Physiological and Molecular Response of Arabidopsis Thaliana (L.) to Nano-particles Cerium and Indium Oxide Exposure. ACS Sustainable Chemical Engineering.1(7): 768–778.

Mehrazar, E., Mahdi, R. and Somayeh, R. (2015). ‘Application of Nano-particles for Pesticides, Herbicides, Fertilizers and Animals Feed Management’. International Journal of Nanoparticles.10: 154-155.

Melika, T., Hania, A. Q., Ali, M. A. Q. and Mahdieh, Y. (2015). The Effects of ZnO Nano-particles on Growth Parameters of Corn (SC704). Stem Fellowship Journal.1(1): 17-20.

Mohammad, K. S., Melik, H. and Tao K. (2019). Plant Growth Stage Influences Heavy Metal Accumulation in Leafy Vegetables of Garden Cress and Sweet Basil.Chemical and Biological Technologies in Agriculture. 6(25): 12–19.

Montazeri, L., Javadpour, J., Bonarkdar, S., Shokrgozar, M. L. and Javadian, S. (2010). Hydrothermal Synthesis and Characterization of Hydroxyapatite and Fluoro-hydroxyapatote Nano-size Powders. Biomedical Materials.5: 7-10.

Muhammad, I., Shahid, U. and Mahmoo, D. (2019). Nanofertilization to Enhance Nutrient Use Efficiency and Productivity of Vegetable Plants. Environmental Science and Pollution Research.27: 473-505.

Musico, Y.. F., Maria, L. P. D., Catherine, M. S. and Debora, F. R. (2013). ‘Improved Removal of Pb2+ from Water using a Polymer Based Grapheme Oxide Nano-composite’. Journal of Material Chemistry.10: 10–39.

Naeem, A., Saifullah, A., Zia-ur-R., M., Aktar, T.; Zia, M. H. and Aslam, M. (2018). Silicon Nutrition Lowers Cd Content of Wheat Cultivars by Regulating Transpiration Rate and Activity of Antioxidant Enzymes. Environmental Pollution. 242: 126–135.

Ngorwe, E. N., Nyambaka, H., Murungi, J. and Tabitha., O. (2014). Effects of Physicochemical Properties on Uptake of Pb and Cd in Tobacco Grown in Medially Polluted Soils. The International Journal of Science and Technology.2(8): 8–12.

Nilwala, K., Nadesh, M., Imalka, M. and Veranja, K. (2011). A Green Slow Release Fertilizer Composition Based on Urea Modified Hydroxyapatite Nano-particles Encapsulated Wood. Current Science.101(2): 1–8.

Piao, X., Huang, D. L., Guang, M. Z. and Cui, L. (2012). Adsorption of Pb2+ by Iron Oxide Nano-particles Immobilized Phanerochaete Chrysosporium: Equillibrium, Kinetic, Thermodynamic and Mechanisms Analysis. Chemical Engineering Journal. 203: 423 - 431.

Pramod, M., Dhoke, S. K. and Khanna, A. S. (2013). Effect of Nano-Zinc Oxide Particle Suspensions on Growth of Mung (Vigna radiata) and Gram (Cicer arietinum) Seedlings Using Plant Agar Method. Journal of Nanotechnology.4: 25-30.

Prasad, T. N., Sudhakar, P., Sajanlal, P. R., Sreenivasulu, Y., Latha, P., Munaswamy, Y., Raja Reddy, K., Sreeprasad, T. S. and Pradeep, T. (2012). Effect of Nano-scale ZnO Particles on the Germination, Growth and Yield of Peanut. Journal of Plant Nutrition.35(6): 905-927.

Qi, L., Lixu, H., Guangy, T., Zhihui, Y. W., Chun, Y., J. T. and Wun, C. H. W. (2020). Simultaneous Immobilization of Pb, Cd and As in Soil by Hybrid Iron-, Sulfate- and Phosphate-based Bionano-composite: Effectiveness, long-term stability and bio-availablity/bio-accessibility evaluation. Chemosphere. 10: 10–19.

Raliya, R., Biswas, P. and Tarafdar, J. C. (2015). Titanium Oxide Nano-particle Bio-synthesis and its Physiological Effect on Mung Bean (Vigna radiata L.). Biotechnology Reports.5: 22-26.

Rameshaiah, G. N., Biswas, P. J. and pallavi, S. (2015). Nanofertilizers and Nanosensors–An attempt for developing smart agriculture. International Journal of Engineering Research and General Science. 3(1): 314–320.

Rezvani, N., Sorooshzadeh, A. and Farhadi, N. (2012). Effect of Nanosilver on Growth of Saffron in Flooding Stress. World Academic Science Engineering Technology.1: 517–522.

Rizwan, M., Ali, Q., Farid, M., Hussain, A., Ali, S., Shakoor, M. B., Rehman, M. Z. U. and Asma, M. (2017). Effect of Zinc Lysine on Growth, Yield and Cd Uptake in Wheat (Triticum aestivum L.) and Health Risk Assessment. Chemosphere. 187: 35–42.

Rizwan, M., Ali, S., Alyemeni, M. N., Rehman, M. Z., Malik, S., Adrees, M., Qayyum, M. F., Alamri, S. A. and Ahmad, P. (2019). Effect of Foliar Applications of Silicon and Titanium (IV) Oxide Nano-particles on Growth, Oxidative Stress, and Cadmium Accumulation by Rice (Oryza sativa). Acta Physiol. Plant.41: 35-43.

Saghi A, Rashed M. H. and Mohassel,. M. P. (2016). Phyto-remediation of Lead Contaminated Soil by Sinapis arvensis and Rapistrum rugosum. International Journal Phytoremediation. 4: 387–392.

Saifullah, A., Javed, H., Rengel, Z., Naeem, A. and Dahlawi, S. (2016). Timing of Foliar Zinc Application Plays a Vital Role in Minimizing Cadmium Accumulation in Wheat Growth. Environmental Science Pollution Resource International. 23: 16432–16439.

Sezgin, N., Farhan, M., Fatima, A. and Awan, N. (2019). Comparative Analysis of Cr and Cd in Various Parts of Wheat and Maize. Pollution Journal of Environmental Studies. 28: 1561–1566.

Shalaby, T. A., Alshaal, T., Bayoumi, Y., Abdalla, N., Taha, H., Shehata, S., Amer, M. and Domokos-Szabolcsy, É. H. (2016). Nano-particles, Soils, Plants and Sustainable Agriculture. In: Shivendu R., Nandita D., Eric L., editors. Nanoscience in Food and Agriculture. 1: 283–312.

Shojaei, T. R., Salleh, M. A., Mobli, H., Tabatabaei, M., Aghbashlo, M., Rashid, S. A. and Tan, T. (2019). Applications of Nano-technology and Carbon Nano-particles in Agriculture. In synthesis, technology and applications of carbon nano-materials; Suraya, A. R., Raja, N. I. R. O., Mohd, Z. H., Eds.; Elsevier: 214: 247–277.

Singh, N. B, Sonal, A.,Garima, N. and Rachna, C. (2018). Water Purification by Using Adsorbents: The review. Environmental Technology & Innovation. 11: 187 - 240.

Song, U., Shin, M., Kim, Y., Lee, G., Roh, J. and Lee, E. J. (2013). Functional Analysis of Titanium Dioxide Nano-particle Toxicity in Three Plant Species. Biological Trace Element Research. 155(1): 93-103.

Srivastava, G., Kusurkar, T. S., Roy, M., Airan, S., Sharma, R. K., Singh, S. K., Sarkar, S. and Das, M. (2014). Iron Pyrite, a Potential Photo-voltaic Material, Increases Plant Biomass upon Seed Pre-treatment. Material Express. 4: 23–31.

Suchanek, K., Marta, M., Amenda, B., Marcin, P., Maciej, S. and Simka, S. (2019). Electro-chemical Properties and Bio-activity of Hydroxyapatite Coatings Prepared by MEA/EDTA Double-regulated Hydrothermal Synthesis. Electrochemical Acta. 298: 685-693.

Sun, J., Fan, Q., Wu, L., Ma, J., Cui, L., Quan, G., Yan, J., Hina, K., Abdul, B. and Wang, H.. (2020). Effects of Nano-biochar on Cadmium Uptake in Vegetables and its Natural Downward Movement in Saline Alkali Soil. Environmental Pollution Bioavailability.32: 36–46.

Tarafdar, J. C., Mahawar, H., Raliya, R. and Rathore, I. (2014). Development of Zn Nanofertilizer to Enhance Crop Production in Pearl Millet (Pennisetum americanum). Agricultural Research. 3(3): 257–262.

Tarafder, C., Mahbuba, D., Morshed, A., Rakibul, I., Ripon, A., Jahidul, I., Sohel, A., Mohamed, A. S. A. and Zaved, H. K. (2020). Formulation of a Hybrid Nano-fertilizer for Slow and Sustainable Release of Micro-nutrients. ACS Omega. 5: 23960−23966.

Wang, S. H., Gao, S. C., Wang, F. Y. and Wang, X. G. (2016). Heavy Metal Accumulation in Different Rice Cultivars as Influenced by Foliar Application of Nanosilicon. Water Air Soil Pollution.213: 227–228.

Willer, H. and Lernoud, J. (2015). The World of Organic Agriculture, Summarry In: RIOA FiBL & IFOAM: The World of Organic Agriculture. Statistics and Emerging Trends. 24-30.

Wu, S. G., Huang, L., Kong, I. C., Head, J., Chen, D. R. and Tang, Y. J. (2012). Phyto-toxicity of Metal Oxide Nano-particles is Related to Both Dissolved Metals Ions and Adsorption of Particles on Seed Surface. Journal of Petroleum Environmental Biotechnology.3: 126-127.

Yaoyao, W., Fuping, J., Yukui, R., Chuanxin, M., Yukui, R., Daniel, C. and Baoshan, X. (2019). Effect of Metal Oxide Nano-particles on Heavy Metal and Amino Acids in Wheat Grains (Triticum aestivum) in a life-cycle study. Journal of Environmental Management.241: 319-327.

Yong, E. K., Jung, K. K., Young, K. and Joong, K. (2019). Development of SEM and STEM-in-SEM Grid Holders for EDS Analysis and Their Applications to Apatite Phases. Journal of Analytical Science and Technology. 49: 428-434.

Yuvakkumar, R., Elango, V., Kannan, N. S., Rajendran, V. and Prabu, P. (2011). Influence of Nano-silica Powder on the Growth of Maize Crop (Zea Mays L.). International Journal of Green Nanotechnology.3(3): 80–190.

Zahra, S. K., Muhammad, R., Shafaqat, A., Muhammad, R. J. and Muhammad, A. (2019). The Accumulation of Cd in Wheat (Triticum aestivum) as Influenced by ZnO Nano-particles and Soil Moisture Conditions. Environmental Science and Pollution Research.26(9): 19859-19870.

Zhang, V., Edward, B. S., Oancea, F., Kurpad, A. l., Sicuia, O. A., Constantinescu, F. and Dinu, S. (2019). Responsive Nano-polymers for Crop Protection and Growth. Polymers. 2: 229–251.

Zhangwei, L, Li, C., Man, M., Zhou, Z. and Wang, L. (2019). The Research of Nano-particle and Micro-particle Hydroxyapatite Amendment in Multiple Heavy Metals Contaminated Soil Remediation. JOURNAL OF NANOTECHNOLOGY. 4: 92–123.

Zhou, Z., Liang, X., Zhang, B., Liu, H., Ma, W., Shi, Z. and Yang, S. (2019). Zn Effects on Cd Toxicity in Two Wheat Varieties (Triticum aestivum L.) Differing in Grain Cadmium Accumulation. Ecotoxicological Environmental Safety. 183: 109562.

Zhu, Y, Xu, F. and Liu,. Q. (2019). Nano-materials and Plants: Positive Effects, Toxicity and the Remediation of Metal and Metalloid Pollution in Soil. Science Total Environment..662: 414–421.

# APPENDICES

## Appendix I: Percentage Pb and Cd reduction uptake in kales, spinach and beans at maturity (After 90 days)

| TREATMENT |  | % Pb Reduction n=9 |  |  |  |  | % Cd Reduction n=9 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Kales | spinach | Beans |  |  | Kales | spinach | Beans |
| Bone nHA |  | 86.82 | 88.40 | 92.51 |  | 87.60 |  | 87.98 | 90.36 |
| Syn nHA |  | 78.74 | 80.01 | 87.78 |  | 83.71 |  | 81.86 | 87.25 |
| Bone nHA +DAP |  | 80.38 | 79.68 | 90.72 |  | 85.77 |  | 86.03 | 83.13 |
| Syn nHA +DAP |  | 76.10 | 75.84 | 86.64 |  | 79.57 |  | 80.62 | 76.77 |
| Bone nHA+ NPK |  | 77.45 | 80.84 | 85.43 |  | 76.19 |  | 87.64 | 81.51 |
| Syn nHA+ NPK |  | 74.22 | 75.28 | 80.88 |  | 72.07 |  | 76.46 | 69.68 |
| Bone nHA+DAP+NPK |  | 80.41 | 78.72 | 92.47 |  | 81.39 |  | 86.98 | 81.55 |
| Syn nHA+DAP+NPK |  | 74.71 | 77.33 | 87.16 |  | 81.53 |  | 79.70 | 74.54 |
| DAP |  | -43.43 | -7.99 | -18.20 |  | -28.22 |  | -29.58 | -41.89 |
| NPK |  | -43.14 | -12.76 | -26.09 |  | -23.98 |  | -31.51 | -25.50 |
| DAP+NPK |  | -16.37 | -8.086 | -17.14 |  | -24.78 |  | -28.53 | -29.45 |
| Non-treated control |  | 0.00 | 0.00 | 0.00 |  | 0.00 |  | 0.00 | 0.00 |
| P-value |  | ˂0.01 |  |  |  |  | ˂0.01 |  |  |

## Appendix II: Percentage effect on height growth performance of kales, spinach and beans at maturity (After 90 days)

| TREATMENT | % increase in kales heights |  | % increase in spinach heights |  | % increase in beans heights |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Synthetic nHA | Bone nHA | Synthetic nHA | Bone nHA | Synthetic nHA | Bone nHA |
| nHA | 149.55 | 154.55 | 100.00 | 123.35 | 179.47 | 202.40 |
| nHA +DAP | 158.29 | 165.67 | 103.35 | 116.65 | 184.31 | 197.67 |
| nHA+ NPK | 112.64 | 216.15 | 65.00 | 146.65 | 165.01 | 167.10 |
| nHA+DAP-NPK | 104.86 | 166.67 | 50.00 | 125.0 | 163.82 | 185.92 |
| DAP | 30.12 | 39.40 | 6.65 | 20.00 | 49.37 | 43.56 |
| NPK | 23.30 | 35.36 | 6.65 | 46.65 | 56.60 | 60.00 |
| DAP-NPK | 32.04 | 41.42 | 16.75 | 41.65 | 69.85 | 62.37 |
| Non-treated control | 0.0d | 0.0c | 0 | 0 | 0 | 0 |
| P-value | ˂0.01 | ˂0.01 | ˂0.01 | ˂0.01 | ˂0.01 | ˂0.01 |

## Appendix III: % Phosphate release rate in bone and synthetic nHA nano-fertilizer

Figure 4.14: % Nitrate release rate in DAP fertilizer and nano-fertilizers with increase in number of days

## Appendix IV: % Phosphate release rate in bone and synthetic nHA nano-fertilizer

Figure 4.15: % Phosphate release rate in DAP fertilizer and nano-fertilizers with increase in number of days

## Appendix V: Published paper With IOSR-JAC.

Effects On Nanofertilizers On Cd and Pb Uptake In Kales Grown In Medially Polluted Experimental Soil. Ngorwe .E.N., Nawiri M., Murungi J., Nyambaka H. and Ongera T. 1,2,3,4,5(Chemistry Department, Kenyatta University, Kenya)

Abstract

Background: Most agriculturalists use excess commercial fertilizers with the notion that some will be eroded and leached eventually causing eutrophication and alters soil pH that increases Cd and Pb uptake in crops .Nanoparticles have numerous adsorption sites that reduce Cd and Pb uptake in crops and it has controlled release of nutrients guaranteeing longer interaction with the crops to ensure safer and higher crop yields to feed sporadic growing population.

Materials and Methods: This study uses nanohydroxyapatite adsorbents from waste bones to synthesis nanofertilizers by encapsulating with DAP and NPK commercial fertilizers. Pots study in green house for contaminated soils were conducted with eight treatments in triplicate; DAP added, NPK added, NPK-DAP added, DAP nanofertilizer, NPK nanofertilizer, NPK-DAP nanofertilizer and non-treated control (ck) treatments, for sukuma wiki (kales) in Kitutu Chache south sub-county, Kisii County, Kenya. Nine pots were set for each treatment with one seedling each planted per pot. Nanofertilizers were applied at normal application rates during planting. Crops were left grown for 30 days to 90 days until they matured and harvested three times on a monthly basis. Harvested leaves were washed with distilled deionized water, oven dried and then acid digested and then analyzed by AAS for Cd and Pb. Data obtained was analyzed by ANOVA and t-test to compare means of various treatment, Cd and Pb in contaminated soils.

Results: The nanofertilizers treatment recorded lowest levels of Cd and Pb in sukuma wiki harvested leaves. The bone ash (nHA added) had the lowest concentration levels of Cd (18.14±0.29) and Pb (15.91±0.57) with NPK nanofertilizers also recording lower concentration levels of Cd (27.29±0.50) and Pb (21.59±0.74). The DAP added fertilizers recorded highest concentration levels of Pb (56.74±5.75) while NPK added fertilizers recorded highest concentration levels of Cd (53.46±2.55). The bone nanofertilizer grown sukuma wiki had higher growth performance and lower levels of Cd and Pb to the permissible levels allowed by WHO/FAO in Kenyan vegetables. The bone ash nano treatment posted the lower heavy metals concentration levels of Cd (18.14±0.29) and Pb (15.91±0.57) while in synthetic experiments leaves harvested from synthetic ash nanofertilizer treated pots had Cd (23.71±1.92) and Pb (14.60±0.30). Cadmium concentration levels in kales harvested from bone ash recorded the highest reduction of 60.69% as compared with the non-treated control followed by bone NPK nanofertilizer with 30.70% cadmium uptake reduction. Lead uptake in bone set-up was most efficiently reduced by bone ash (nHA) by 59.25% while reduction by same treatment in synthetic experiment was 58.71%. The bone NPK nanofertilizer had 44.70% lead uptake reduction. However fertilizer amendment increased lead uptake with DAP added treatment hiking lead uptake in kales by 14.04%.

Conclusion: The result is recommended for nanofertilizers to be used in growing other crops such as maize, beans, spinach potatoes, wheat, rice and other vegetative crops in medially polluted soils, especially in peri-urban farming to boost food productivity to feed ever growing population.

Key Word: Nanofertilizer; Amendment; Uptake; Nanohydroxyapatite; Bone Ash.

## Appendix VI: Published paper With IJSR

Efficacy of Nanofertilizers on Spinach Growth Performance in Medially Polluted Soils

Ngorwe .E.N., Nyambaka H., Murungi J., Nawiri M., and Ongera T. 1,2,3,4,5(Chemistry Department, Kenyatta University, Kenya)

Abstract

Purpose

Food security has been a global problem with the sporadic growing population especially in the developing world, Kenya included. Many crop growth enhancers have been used such as conventional fertilizers, bio-fertilizers to boost food productivity. However, use excessive commercial fertilizer with the notion that some will be eroded and leached eventually causes eutrophication and alters soil pH that increases heavy metal uptake in crops threatening food safety and it has also minimal plant nutrient utilization. Nanoparticles have been used to give slower and timely release of nutrients to plants due to their versatile desirable characteristics.

Methods

Pot study in green house for contaminated soils were conducted with eight treatments in triplicate; DAP added, NPK added, NPK-DAP added, DAP nanofertilizer, NPK nanofertilizer, NPK-DAP nanofertilizer and non-treated control (ck) treatments, for spinach in the greenhouse study done in Nyakoe, Kisii county. Nine pots were set for each treatment with one seedling each. Nanofertilizers were applied at normal application rates during planting. Spinach plants were left grown for 30 days to 90 days until they matured as the growth performance parameters were being recorded.

Results

The results shows that there was a significant difference in plant growth performance in pots where nanofertilizers were used, with spinach amended with synthetic ash (nHA) increasing the growth parameters as follows; height (64.29%), dry matter weight (17.55%), leaf diameter (34.54%) and number of leaves (32.39%) while bone ash treatment increased height by (65.34%), dry matter weight (17.52%), leaf diameter (44.34%) and number of leaves (37.24%) when compared to NPK-DAP fertilizer added control.

Conclusion

Nanofertilizers enhances the growth performance of crops even when grown in medially polluted sandy loamy soils of lower fertility, especially in peri-urban farming to boost food productivity to feed ever growing population.

Keywords: Nanohydroxyapatite, nanofertilizer, synthetic ash, bone ash, Nanoparticles, growth performance

## Appendix VII: Approval of Research Proposal

## Appendix VIII: Research Authorization